Mt. Morgan SITE PROCEDURE

Plant Surveys and Circuit Performance Assessment

Standard Work Procedure  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | HM-PRC-VXX-PRO207 |
| --- | --- |
| Title | Plant Surveys and Circuit Performance Assessment |
| Scope | Plant surveys and circuit performance assessment - survey planning and execution, flow and density verification, screen and cyclone performance, residence time, leach, CIL and adsorption profiles, thickener performance, elution assessment, dosing verification, screen efficiency, carbon and resin loss, and oxygen utilisation. |
| Register area | 203 Plant Surveys, on tabs JSEA_MET and SWI-MET |
| Hazard analyses beneath | 12 (JSEA-PRO-MET-203-001 to -012) |
| Work instructions beneath | 12 |
| Process owner | Heritage Mineral Operations · Business unit Mt. Morgan |
| Document owner | Process Operations Superintendent |
| Document approver | Process Manager |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  PURPOSE / SCOPE

This procedure covers plant surveys and circuit performance assessment at the Mt. Morgan processing plant. It is the procedure that the 12 hazard analyses and 12 work instructions in register area 203 sit under.

Plant surveys and circuit performance assessment - survey planning and execution, flow and density verification, screen and cyclone performance, residence time, leach, CIL and adsorption profiles, thickener performance, elution assessment, dosing verification, screen efficiency, carbon and resin loss, and oxygen utilisation.

# 2  RESPONSIBILITIES

| Role | Responsibilities |
| --- | --- |
| Operator / Metallurgical Technician / Met Lab Technician | Carry out the task to the schedule and to the work instruction. Only carry out work where competent and authorised to do so. Record what was actually done. Work not done is recorded as not done - never invented and never back-filled. Stop and report if any control in the JSEA is not in place. |
| Shift Supervisor / Coordinator | Authorise the task and confirm the area is fit before it starts. Know that the task is in progress and where the person is. Understand that much of the plant is automated and equipment may start or stop without warning. Act on any off-specification result reported from the task. |
| Metallurgist | Set and maintain the schedule - what is done, how often, and what is reported. Review the results and act on the trends. Investigate any variance outside the agreed tolerance before a period is closed. |
| Process Manager / Superintendent | Ensure all personnel are trained and competent. Ensure this procedure and the documents beneath it are reviewed at the stated interval. Approve the risk ranking in the JSEAs. |

# 3  ABBREVIATIONS / DEFINITIONS

| Term | Meaning |
| --- | --- |
| JSEA | Job safety and environmental analysis - one per task, giving the step-by-step hazards, controls and risk ranking. |
| SWI | Standard work instruction - one per task, giving the step-by-step method. |
| SWP | Standard work procedure - this document. |
| Steady state | Normal operation held for at least 15 to 20 minutes. |
| ReCYN | The resin-in-pulp cyanide and metal recovery process in Areas 041, 051, 071 and 081. |
| CN Free / WAD CN | Free cyanide by silver nitrate titration; weak acid dissociable cyanide by distillation. |

# 4  POTENTIAL HAZARDS

The step-by-step hazard analysis for each task, with the risk ranking, is in the JSEA for that task. The hazards common across this area are:

- Hydrogen cyanide gas released at the open sample point

- Splash of cyanide-bearing slurry or solution to skin or eyes

- Fall from a tank top, launder platform, column platform or access ladder

- Working alone in a cyanide area where a collapse would not be seen

- Contact with an agitator, sample cutter, pump or screen that starts without warning

- Slip, trip or fall on wet or slurry-covered walkways around sample points

- Non-representative sample leading to a wrong process decision

- Cross-contamination from a container or cutter not cleaned between points

- Manual handling injury from carrying sample buckets, containers and composite drums

- Hearing damage in the mill, screen, compressor and blower areas

- Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt

- Confined space atmosphere at a tank top hatch, launder or hopper opening

- Contact with hot solution or hot surface at the elution, stripping or regeneration circuits

- Mercury vapour in the gold room, elution and retort areas

# 5  PPE

Standard PPE is worn for all normal operations: hard hat, safety glasses, high-visibility long-sleeved shirt and long trousers, safety boots, and gloves appropriate to the task.

The following is added where the task requires it:

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

- Hearing protection

- Heat-resistant gloves

- Face shield

- Acid-resistant gloves, apron and face shield

- Chemical splash goggles

- Personal multi-gas monitor including H2S, calibrated and in test date

# 6  PROCEDURE

6.1  Introduction

Warning: many operations on the gold processing plant are automated and equipment may start or stop without warning. It is the operator's responsibility to ensure the safety of all personnel working on the plant at all times.

6.2  Procedure and implementation steps

The documents below are the controlled method for each task. This procedure does not repeat them.

| JSEA | Work instruction | Task | Class |
| --- | --- | --- | --- |
| JSEA-PRO-MET-203-001 | SWI-PRO-MET-203-001 | Plant Survey Planning, Permitting and Execution | Safety-critical |
| JSEA-PRO-MET-203-002 | SWI-PRO-MET-203-002 | Slurry Flow, Density and Tonnage Verification Survey | Safety-critical |
| JSEA-PRO-MET-203-003 | SWI-PRO-MET-203-003 | Screen and Cyclone Performance Survey - Size Split Determination | Safety-critical |
| JSEA-PRO-MET-203-004 | SWI-PRO-MET-203-004 | Residence Time and Tracer Test on Leach and Adsorption Trains | Safety-critical |
| JSEA-PRO-MET-203-005 | SWI-PRO-MET-203-005 | Leach and CIL Profile Survey - Tank-by-Tank Gold and Cyanide Profile | Safety-critical |
| JSEA-PRO-MET-203-006 | SWI-PRO-MET-203-006 | Adsorption Profile Survey - Metal and Cyanide Resin Circuits | Safety-critical |
| JSEA-PRO-MET-203-007 | SWI-PRO-MET-203-007 | Thickener Performance Survey - Flux, Bed Level and Flocculant Response | Safety-critical |
| JSEA-PRO-MET-203-008 | SWI-PRO-MET-203-008 | Elution and Electrowinning Batch Performance Assessment | Safety-critical |
| JSEA-PRO-MET-203-009 | SWI-PRO-MET-203-009 | Reagent Dosing Verification and Dosing Pump Calibration Check | Safety-critical |
| JSEA-PRO-MET-203-010 | SWI-PRO-MET-203-010 | Interstage and Safety Screen Efficiency Check and Loss Quantification | Safety-critical |
| JSEA-PRO-MET-203-011 | SWI-PRO-MET-203-011 | Carbon and Resin Loss Quantification Survey | Safety-critical |
| JSEA-PRO-MET-203-012 | SWI-PRO-MET-203-012 | Oxygen Utilisation and Sparger Performance Survey | Safety-critical |

6.3  Schedule

| Task | Frequency |
| --- | --- |
| 203-001 Plant Survey Planning, Permitting and Execution | As required for a performance survey; typically quarterly and after any significant plant change. |
| 203-002 Slurry Flow, Density and Tonnage Verification Survey | Quarterly, and after any instrument replacement or recalibration. |
| 203-003 Screen and Cyclone Performance Survey - Size Split Determination | Quarterly, and after any panel change or aperture change. |
| 203-004 Residence Time and Tracer Test on Leach and Adsorption Trains | Once at commissioning, then after any change to feed rate, agitator or tank configuration. |
| 203-005 Leach and CIL Profile Survey - Tank-by-Tank Gold and Cyanide Profile | Quarterly, and whenever recovery moves without an obvious cause. |
| 203-006 Adsorption Profile Survey - Metal and Cyanide Resin Circuits | Quarterly, and after any change to resin inventory or transfer rate. |
| 203-007 Thickener Performance Survey - Flux, Bed Level and Flocculant Response | Quarterly, and whenever overflow clarity or underflow density moves. |
| 203-008 Elution and Electrowinning Batch Performance Assessment | Every batch, assessed and trended monthly. |
| 203-009 Reagent Dosing Verification and Dosing Pump Calibration Check | Quarterly, and after any dosing pump repair or replacement. |
| 203-010 Interstage and Safety Screen Efficiency Check and Loss Quantification | Monthly, and after any panel replacement. |
| 203-011 Carbon and Resin Loss Quantification Survey | Quarterly, and whenever the inventory reconciliation shows an unexplained loss. |
| 203-012 Oxygen Utilisation and Sparger Performance Survey | Quarterly, and after any sparger clean or replacement. |

# 7  FLOWCHART

Not reproduced here. Each work instruction carries its own step sequence in Section 6.

# 8  TRAINING

Every person carrying out a task in this area is trained and signed off against the work instruction for that task, and has signed on to the matching JSEA at a communication session.

- Site induction, current.

- Cyanide awareness and gas detection competency where the area requires it.

- Working at height competency where the task requires it.

- Competency in the determinations, instruments and calculations used in the task.

- Refresher at the interval set by the site training matrix, and after any change to the instruction.

# 9  REFERENCE

- KBK-MIR-MP-PRO-MET-SOP-0027 Grinding Survey, received 11 Aug 2026 - a worked plant survey end to end

- KBK-MIR-MP-PRO-MET-SOP-0047 Pengukuran Profil Lumpur Cyclone Over Flow, received 11 Aug 2026

- 4034-PR-PRO-002 Sampling Protocol

- KBK-MIR-MP-PRO-OPE-SOP-0004 SG Determination by Marcy Scale

- KBK-MIR-MP-PRO-MET-SOP-0045 Pengukuran Densitas Lumpur, received 11 Aug 2026

- 4034-002-VE-025 McLanahan rotary scrubber IO&M and 4034-001-VE-038 IsaMill control philosophy, both received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0008 Cyclone Efficiency

- KBK-MIR-MP-PRO-MET-SOP-0029 Sizing Harian COF and SOP-0020 Distribusi Logam dan Ukuran, both received 11 Aug 2026

- MM-4034-033 Screen Aperture Register

- 4034-004-VE-025 and 4034-011-VE-022 Goldquip screen manuals, received 11 Aug 2026

- No direct source held. Written from first principles.

- Plant Operating Manual Sections 3.4 and 3.5 - train configuration and design residence time

- 4034-PR-PRO-002 Sampling Protocol, Leach Area table

- KBK-MIR-MP-PRO-MET-SOP-0019 Profil Leaching and SOP-0048 leach tank sampling and profile, both received 11 Aug 2026

- HM-PRC-V01-PRO004 Leach Circuit and PRO005 Carbon in Leach

- 4034-PR-PRO-002 Sampling Protocol, ReCYN Adsorption table

- KBK-MIR-MP-PRO-MET-SOP-0049 resin tank sampling and profile and SOP-0058 resin PSD, both received 11 Aug 2026

- KBK SOP-PROC-CNREC-01 Resin transfer between adsorption tanks, received 11 Aug 2026

- HM-PRC-V01-PRO006 and PRO007

- Tail Thickener and Cu Thickener Field Operator Procedures

- 4034-018A-VE-007 Roytec tails thickener control philosophy and 4034-018A-VE-045 IOM, both received 11 Aug 2026 - rake torque, bed level and underflow density limits

- 4034-019-VE-006 Model 01 and 4034-019B-VE-007 Model 05 Roytec flocculant control philosophies, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0014 Settling Test

- HM-PRC-V01-PRO008 and PRO016

- 4034-013-VE-028 Applied Heat Thermomat 2300 O&M manual, received 11 Aug 2026 - strip temperatures and circuit design conditions

- 4034-014-VE-004 and -019 Stantil carbon regeneration kiln control philosophy and IOM, received 11 Aug 2026

- HM-PRC-V01-PRO011 Gold Elution and PRO013 Gold Electrowinning

- HM-PRC-V01-PRO021 to PRO027 reagent procedures

- HM-PP-006B Reagents Consumption 2026 - design dose rates

- 4034-046-VE-019 Transmin quicklime slaking plant functional description, received 11 Aug 2026

- RA-01 Resin Loss and RA-02 Carbon Contamination Registers Rev A

- KBK-MIR-MP-PRO-MET-SOP-0028 Sizing Harian CIL Tail, received 11 Aug 2026

- SWI-PRO-OPR-032-003, -004 and -005 screen instructions, issued

- RA-01 Resin Loss Register and RA-02 Carbon Contamination Register Rev A, and their study reports

- MM-4034-033-RES Resin Line Schedule (268 lines)

- KBK-MIR-MP-PRO-MET-SOP-0058 Distribusi Ukuran Partikel Resin, received 11 Aug 2026

- 4034-044-VE-003 Rev B Glencore Hypersparge supersonic gas sparger installation and operating instructions, received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0046 Pengukuran Oksigen Terlarut, received 11 Aug 2026

- HM-PRC-V01-PRO004 Leach Circuit and SWI-PRO-OPR-031-004 Oxygen Sparger Inspection and Cleaning

# 10  REVIEW

This procedure and the documents beneath it are reviewed every 12 months, and immediately after any incident, plant change, equipment change or change to the schedule.

# 11  REGISTER TRACEABILITY

The three-digit suffix is shared between the two registers, so SWI-PRO-MET-203-011 is the work instruction for JSEA-PRO-MET-203-011.

Registers: HM-MMM-WHS-REG-JSEA-PRO-updated_10.xlsx tab JSEA_MET, and HM-MMM-WHS-REG-XXX-R00-SWI-SWMS.xlsx tab SWI-MET. GGT working masters are MM-4034-033-OR-03-JSEA-Register-RevE.xlsx and MM-4034-033-OR-03-SWI-Register-RevE.xlsx.

| Item | Count |
| --- | --- |
| Register lines in area 203 | 12 |
| Hazard analyses issued | 12 |
| Work instructions issued | 12 |
| Desk-based tasks with a JSEA but no work instruction | 0 |
| Safety-critical | 12 |
| Issued but NOT FOR USE | 0 |