Mt. Morgan SITE PROCEDURE

Metallurgical Laboratory Physical Testwork

Standard Work Procedure  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | HM-PRC-VXX-PRO208 |
| --- | --- |
| Title | Metallurgical Laboratory Physical Testwork |
| Scope | Metallurgical laboratory physical testwork - sample receipt, sizing by wet and dry screening, density and specific gravity, moisture, suspended solids, rheology, settling, filtration, Bond work index, grind establishment, carbon and resin sizing, and the operation of the physical testwork equipment. |
| Register area | 204 Met Lab - Physical Testwork, on tabs JSEA_MET and SWI-MET |
| Hazard analyses beneath | 19 (JSEA-PRO-MET-204-001 to -019) |
| Work instructions beneath | 19 |
| Process owner | Heritage Mineral Operations · Business unit Mt. Morgan |
| Document owner | Process Operations Superintendent |
| Document approver | Process Manager |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  PURPOSE / SCOPE

This procedure covers metallurgical laboratory physical testwork at the Mt. Morgan processing plant. It is the procedure that the 19 hazard analyses and 19 work instructions in register area 204 sit under.

Metallurgical laboratory physical testwork - sample receipt, sizing by wet and dry screening, density and specific gravity, moisture, suspended solids, rheology, settling, filtration, Bond work index, grind establishment, carbon and resin sizing, and the operation of the physical testwork equipment.

# 2  RESPONSIBILITIES

| Role | Responsibilities |
| --- | --- |
| Operator / Metallurgical Technician / Met Lab Technician | Carry out the task to the schedule and to the work instruction. Only carry out work where competent and authorised to do so. Record what was actually done. Work not done is recorded as not done - never invented and never back-filled. Stop and report if any control in the JSEA is not in place. |
| Shift Supervisor / Coordinator | Authorise the task and confirm the area is fit before it starts. Know that the task is in progress and where the person is. Understand that much of the plant is automated and equipment may start or stop without warning. Act on any off-specification result reported from the task. |
| Metallurgist | Set and maintain the schedule - what is done, how often, and what is reported. Review the results and act on the trends. Investigate any variance outside the agreed tolerance before a period is closed. |
| Process Manager / Superintendent | Ensure all personnel are trained and competent. Ensure this procedure and the documents beneath it are reviewed at the stated interval. Approve the risk ranking in the JSEAs. |

# 3  ABBREVIATIONS / DEFINITIONS

| Term | Meaning |
| --- | --- |
| JSEA | Job safety and environmental analysis - one per task, giving the step-by-step hazards, controls and risk ranking. |
| SWI | Standard work instruction - one per task, giving the step-by-step method. |
| SWP | Standard work procedure - this document. |
| Steady state | Normal operation held for at least 15 to 20 minutes. |
| ReCYN | The resin-in-pulp cyanide and metal recovery process in Areas 041, 051, 071 and 081. |
| CN Free / WAD CN | Free cyanide by silver nitrate titration; weak acid dissociable cyanide by distillation. |

# 4  POTENTIAL HAZARDS

The step-by-step hazard analysis for each task, with the risk ranking, is in the JSEA for that task. The hazards common across this area are:

- Cross-contamination from a container or cutter not cleaned between points

- Hydrogen cyanide gas released at the open sample point

- Manual handling injury from carrying sample buckets, containers and composite drums

- Non-representative sample leading to a wrong process decision

- Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt

- Hearing damage in the mill, screen, compressor and blower areas

- Contact with an agitator, sample cutter, pump or screen that starts without warning

- Splash of cyanide-bearing slurry or solution to skin or eyes

- Cuts from broken glassware, and burns from hot glassware

- Contact with hot solution or hot surface at the elution, stripping or regeneration circuits

- Release from a pressurised sample line, hose or fitting

- Contact with sulphuric or hydrochloric acid - burn to skin or eyes

# 5  PPE

Standard PPE is worn for all normal operations: hard hat, safety glasses, high-visibility long-sleeved shirt and long trousers, safety boots, and gloves appropriate to the task.

The following is added where the task requires it:

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

# 6  PROCEDURE

6.1  Introduction

Warning: many operations on the gold processing plant are automated and equipment may start or stop without warning. It is the operator's responsibility to ensure the safety of all personnel working on the plant at all times.

6.2  Procedure and implementation steps

The documents below are the controlled method for each task. This procedure does not repeat them.

| JSEA | Work instruction | Task | Class |
| --- | --- | --- | --- |
| JSEA-PRO-MET-204-001 | SWI-PRO-MET-204-001 | Met Lab Sample Receipt, Logging and Storage | Operating |
| JSEA-PRO-MET-204-002 | SWI-PRO-MET-204-002 | Wet Screening and Sizing Analysis | Operating |
| JSEA-PRO-MET-204-003 | SWI-PRO-MET-204-003 | Particle Size Distribution by Laser Sizer | Operating |
| JSEA-PRO-MET-204-004 | SWI-PRO-MET-204-004 | Slurry Density Determination by Marcy Scale | Operating |
| JSEA-PRO-MET-204-005 | SWI-PRO-MET-204-005 | Solids Specific Gravity by Pycnometer | Operating |
| JSEA-PRO-MET-204-006 | SWI-PRO-MET-204-006 | Moisture Content Determination | Operating |
| JSEA-PRO-MET-204-007 | SWI-PRO-MET-204-007 | Total Suspended Solids Determination | Operating |
| JSEA-PRO-MET-204-008 | SWI-PRO-MET-204-008 | Slurry Viscosity and Rheology Test | Operating |
| JSEA-PRO-MET-204-009 | SWI-PRO-MET-204-009 | Static and Dynamic Settling Test | Operating |
| JSEA-PRO-MET-204-010 | SWI-PRO-MET-204-010 | Flocculant Screening and Dose Optimisation Test | Operating |
| JSEA-PRO-MET-204-011 | SWI-PRO-MET-204-011 | Filter Press Simulation and Cake Filtration Test | Operating |
| JSEA-PRO-MET-204-012 | SWI-PRO-MET-204-012 | Bond Ball Mill Work Index Test | Operating |
| JSEA-PRO-MET-204-013 | SWI-PRO-MET-204-013 | Grind Establishment Test | Operating |
| JSEA-PRO-MET-204-014 | SWI-PRO-MET-204-014 | Carbon Particle Size Distribution and Fines Determination | Operating |
| JSEA-PRO-MET-204-015 | SWI-PRO-MET-204-015 | Resin Particle Size Distribution and Fines Determination | Operating |
| JSEA-PRO-MET-204-016 | SWI-PRO-MET-204-016 | Dry Sieve Analysis - Ro-Tap RX29 and 200 mm Sieve Set | Operating |
| JSEA-PRO-MET-204-017 | SWI-PRO-MET-204-017 | Sieve Cleaning, Integrity Check and Aperture Verification | Operating |
| JSEA-PRO-MET-204-018 | SWI-PRO-MET-204-018 | Vacuum Filtration of Test Products | Operating |
| JSEA-PRO-MET-204-019 | SWI-PRO-MET-204-019 | Centrifuge Operation for Solution Clarification | Operating |

6.3  Schedule

| Task | Frequency |
| --- | --- |
| 204-001 Met Lab Sample Receipt, Logging and Storage | Every delivery from the plant. |
| 204-002 Wet Screening and Sizing Analysis | Per the sampling schedule; daily on CIL tail and cyclone overflow. |
| 204-003 Particle Size Distribution by Laser Sizer | To be set once the instrument is resolved. |
| 204-004 Slurry Density Determination by Marcy Scale | Every slurry sample requiring a density. |
| 204-005 Solids Specific Gravity by Pycnometer | On each new ore type, and quarterly on plant feed. |
| 204-006 Moisture Content Determination | Every solid sample requiring a dry mass. |
| 204-007 Total Suspended Solids Determination | Per the sampling schedule; each shift on thickener overflow. |
| 204-008 Slurry Viscosity and Rheology Test | On each new ore type, and whenever pumping or mixing behaviour changes. |
| 204-009 Static and Dynamic Settling Test | On each new ore type, and whenever thickener performance changes. |
| 204-010 Flocculant Screening and Dose Optimisation Test | On each new ore type and when a flocculant change is proposed. |
| 204-011 Filter Press Simulation and Cake Filtration Test | On each new ore type and whenever plant cake moisture moves. |
| 204-012 Bond Ball Mill Work Index Test | On each new ore type or ore blend. |
| 204-013 Grind Establishment Test | On each new ore type, and when a change to the grind target is proposed. |
| 204-014 Carbon Particle Size Distribution and Fines Determination | Monthly, and after every regeneration campaign. |
| 204-015 Resin Particle Size Distribution and Fines Determination | Monthly, and after any osmotic shock event or conditioning batch. |
| 204-016 Dry Sieve Analysis - Ro-Tap RX29 and 200 mm Sieve Set | As required by the analysis schedule. |
| 204-017 Sieve Cleaning, Integrity Check and Aperture Verification | After every use for cleaning; quarterly for integrity and aperture verification. |
| 204-018 Vacuum Filtration of Test Products | Every test requiring solid and solution separation. |
| 204-019 Centrifuge Operation for Solution Clarification | As required by the analysis schedule. |

# 7  FLOWCHART

Not reproduced here. Each work instruction carries its own step sequence in Section 6.

# 8  TRAINING

Every person carrying out a task in this area is trained and signed off against the work instruction for that task, and has signed on to the matching JSEA at a communication session.

- Site induction, current.

- Cyanide awareness and gas detection competency where the area requires it.

- Working at height competency where the task requires it.

- Competency in the determinations, instruments and calculations used in the task.

- Refresher at the interval set by the site training matrix, and after any change to the instruction.

# 9  REFERENCE

- KBK-MIR-LAB-PRE-SOP-001 Penerimaan Sampel and PRE-SOP-002 Sortir Sampel

- 4034-PR-PRO-002 Sampling Protocol

- KBK-MIR-LAB-PRE-SOP-008 Uji Kehalusan Sampel

- KBK-MIR-MP-PRO-MET-SOP-0020 Distribusi Logam dan Ukuran, SOP-0028 Sizing Harian CIL Tail and SOP-0029 Sizing Harian COF, all received 11 Aug 2026

- ILS quotation Q0023979 - Ro-Tap RX29, sound enclosure and twelve 200 mm sieves 38 um to 2 mm

- No source held. No laser sizer in ILS quotation Q0023979.

- KBK-MIR-MP-PRO-OPE-SOP-0004 SG Determination by Marcy Scale

- KBK-MIR-MP-PRO-MET-SOP-0045 Pengukuran Densitas Lumpur, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0015 SG solid determination by pycnometer

- KBK-MIR-MP-PRO-OPE-SOP-0022 Moisture Content

- KBK-MIR-MP-PRO-MET-SOP-0032 Moisture Content, Bahasa master received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0017 Total Suspended Solid

- KBK-MIR-LAB-ENV-SOP-072 Analisa TSS Gravimetri

- KBK-MIR-MP-PRO-OPE-SOP-0016 Uji Viskositas

- KBK-MIR-MP-PRO-OPE-SOP-0014 Uji Pengendapan

- 4034-018A-VE-007 Roytec tails thickener control philosophy, received 11 Aug 2026

- 4034-019-VE-006 Roytec Model 01 and 4034-019B-VE-007 Model 05 flocculant plant control philosophies, received 11 Aug 2026 - the plant make-up concentration and dose basis

- KBK-MIR-MP-PRO-OPE-SOP-0023 Filter Press

- ILS quotation Q0023979 - Becker VT4.8 oil-free pump, 4-place manifold and filter flasks

- KBK SOP-PROC-CNREC-09 Filtration of copper precipitation, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0006 Uji Bond Work Index (BWI)

- KBK-MIR-MP-PRO-OPE-SOP-0012 Uji Pengujian Grind Establishment

- KBK-MIR-MP-PRO-MET-SOP-0027 Grinding Survey, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0013 Distribusi Ukuran Partikel Karbon Aktivasi

- KBK-MIR-MP-PRO-MET-SOP-0058 Distribusi Ukuran Partikel Resin, received 11 Aug 2026

- ILS quotation Q0023979 - 200 mm sieve set 38 um to 2 mm and Ro-Tap RX29

- RA-01 Resin Loss Register Rev A

- ILS quotation Q0023979 - Ro-Tap RX29 shaker, sound enclosure and twelve 200 mm sieves

- ILS quotation Q0023979 - ultrasonic sieve cleaner FSS Sieve 200 DH

- No cleaning or aperture verification procedure was held before this revision

- ILS quotation Q0023979 - Becker VT4.8, 4-place manifold, four filter flasks and Buchner funnels

- ILS quotation Q0023979 - Ohaus FC5706 centrifuge and 15 mL tubes

- No procedure was held for this instrument before this revision

# 10  REVIEW

This procedure and the documents beneath it are reviewed every 12 months, and immediately after any incident, plant change, equipment change or change to the schedule.

# 11  REGISTER TRACEABILITY

The three-digit suffix is shared between the two registers, so SWI-PRO-MET-204-011 is the work instruction for JSEA-PRO-MET-204-011.

Registers: HM-MMM-WHS-REG-JSEA-PRO-updated_10.xlsx tab JSEA_MET, and HM-MMM-WHS-REG-XXX-R00-SWI-SWMS.xlsx tab SWI-MET. GGT working masters are MM-4034-033-OR-03-JSEA-Register-RevE.xlsx and MM-4034-033-OR-03-SWI-Register-RevE.xlsx.

| Item | Count |
| --- | --- |
| Register lines in area 204 | 19 |
| Hazard analyses issued | 19 |
| Work instructions issued | 19 |
| Desk-based tasks with a JSEA but no work instruction | 0 |
| Safety-critical | 0 |
| Issued but NOT FOR USE | 1 |