Mt. Morgan SITE PROCEDURE

Metallurgical Laboratory Chemical and Leach Testwork

Standard Work Procedure  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | HM-PRC-VXX-PRO209 |
| --- | --- |
| Title | Metallurgical Laboratory Chemical and Leach Testwork |
| Scope | Metallurgical laboratory chemical and leach testwork - cyanide, caustic, acid and chloride titration, lime availability and demand, bottle roll and diagnostic leach testwork, adsorption testwork on carbon and resin, precipitate determination, standard solution preparation and automatic titrator operation. |
| Register area | 205 Met Lab - Chemical and Leach Testwork, on tabs JSEA_MET and SWI-MET |
| Hazard analyses beneath | 19 (JSEA-PRO-MET-205-001 to -019) |
| Work instructions beneath | 19 |
| Process owner | Heritage Mineral Operations · Business unit Mt. Morgan |
| Document owner | Process Operations Superintendent |
| Document approver | Process Manager |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  PURPOSE / SCOPE

This procedure covers metallurgical laboratory chemical and leach testwork at the Mt. Morgan processing plant. It is the procedure that the 19 hazard analyses and 19 work instructions in register area 205 sit under.

Metallurgical laboratory chemical and leach testwork - cyanide, caustic, acid and chloride titration, lime availability and demand, bottle roll and diagnostic leach testwork, adsorption testwork on carbon and resin, precipitate determination, standard solution preparation and automatic titrator operation.

# 2  RESPONSIBILITIES

| Role | Responsibilities |
| --- | --- |
| Operator / Metallurgical Technician / Met Lab Technician | Carry out the task to the schedule and to the work instruction. Only carry out work where competent and authorised to do so. Record what was actually done. Work not done is recorded as not done - never invented and never back-filled. Stop and report if any control in the JSEA is not in place. |
| Shift Supervisor / Coordinator | Authorise the task and confirm the area is fit before it starts. Know that the task is in progress and where the person is. Understand that much of the plant is automated and equipment may start or stop without warning. Act on any off-specification result reported from the task. |
| Metallurgist | Set and maintain the schedule - what is done, how often, and what is reported. Review the results and act on the trends. Investigate any variance outside the agreed tolerance before a period is closed. |
| Process Manager / Superintendent | Ensure all personnel are trained and competent. Ensure this procedure and the documents beneath it are reviewed at the stated interval. Approve the risk ranking in the JSEAs. |

# 3  ABBREVIATIONS / DEFINITIONS

| Term | Meaning |
| --- | --- |
| JSEA | Job safety and environmental analysis - one per task, giving the step-by-step hazards, controls and risk ranking. |
| SWI | Standard work instruction - one per task, giving the step-by-step method. |
| SWP | Standard work procedure - this document. |
| Steady state | Normal operation held for at least 15 to 20 minutes. |
| ReCYN | The resin-in-pulp cyanide and metal recovery process in Areas 041, 051, 071 and 081. |
| CN Free / WAD CN | Free cyanide by silver nitrate titration; weak acid dissociable cyanide by distillation. |

# 4  POTENTIAL HAZARDS

The step-by-step hazard analysis for each task, with the risk ranking, is in the JSEA for that task. The hazards common across this area are:

- Hydrogen cyanide gas released at the open sample point

- Inhalation of acid fume or reagent vapour at the bench

- Cuts from broken glassware, and burns from hot glassware

- Splash of cyanide-bearing slurry or solution to skin or eyes

- Cross-contamination from a container or cutter not cleaned between points

- Non-representative sample leading to a wrong process decision

- Contact with sodium hydroxide solution - burn to skin or eyes

- Contact with sulphuric or hydrochloric acid - burn to skin or eyes

- Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt

- Contact with an agitator, sample cutter, pump or screen that starts without warning

- Hearing damage in the mill, screen, compressor and blower areas

- Contact with hot solution or hot surface at the elution, stripping or regeneration circuits

- Hydrogen sulphide released from sodium hydrosulphide or from an acidified sulphide stream

- Contact with live electrical equipment at a sample pump, cutter or local control station

# 5  PPE

Standard PPE is worn for all normal operations: hard hat, safety glasses, high-visibility long-sleeved shirt and long trousers, safety boots, and gloves appropriate to the task.

The following is added where the task requires it:

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Acid-resistant gloves, apron and face shield

- Chemical splash goggles

# 6  PROCEDURE

6.1  Introduction

Warning: many operations on the gold processing plant are automated and equipment may start or stop without warning. It is the operator's responsibility to ensure the safety of all personnel working on the plant at all times.

6.2  Procedure and implementation steps

The documents below are the controlled method for each task. This procedure does not repeat them.

| JSEA | Work instruction | Task | Class |
| --- | --- | --- | --- |
| JSEA-PRO-MET-205-001 | SWI-PRO-MET-205-001 | Free Cyanide Titration - Silver Nitrate Method | Safety-critical |
| JSEA-PRO-MET-205-002 | SWI-PRO-MET-205-002 | Caustic Soda Strength Titration | Operating |
| JSEA-PRO-MET-205-003 | SWI-PRO-MET-205-003 | Sulphuric Acid Strength Titration | Safety-critical |
| JSEA-PRO-MET-205-004 | SWI-PRO-MET-205-004 | Sodium Chloride (Chloride) Titration | Operating |
| JSEA-PRO-MET-205-005 | SWI-PRO-MET-205-005 | Lime Availability Test | Operating |
| JSEA-PRO-MET-205-006 | SWI-PRO-MET-205-006 | Lime Addition and Lime Demand Test | Operating |
| JSEA-PRO-MET-205-007 | SWI-PRO-MET-205-007 | Bottle Roll Leach Test - As-Received and Pulverised | Safety-critical |
| JSEA-PRO-MET-205-008 | SWI-PRO-MET-205-008 | Extended and Diagnostic Leach Test | Safety-critical |
| JSEA-PRO-MET-205-009 | SWI-PRO-MET-205-009 | CIL/CIP Sequential Triple Contact Testwork | Safety-critical |
| JSEA-PRO-MET-205-010 | SWI-PRO-MET-205-010 | Carbon Adsorption Capacity and Isotherm Test | Operating |
| JSEA-PRO-MET-205-011 | SWI-PRO-MET-205-011 | Carbon Activity and Ball-Pan Hardness Test | Operating |
| JSEA-PRO-MET-205-012 | SWI-PRO-MET-205-012 | Resin Adsorption Capacity and Kinetics Test | Operating |
| JSEA-PRO-MET-205-013 | SWI-PRO-MET-205-013 | Resin Elution Efficiency and Barren Resin Loading Test | Operating |
| JSEA-PRO-MET-205-014 | SWI-PRO-MET-205-014 | Resin Fouling, Osmotic Shock and Bead Integrity Assessment | Operating |
| JSEA-PRO-MET-205-015 | SWI-PRO-MET-205-015 | Cyanide Destruction (Detox) Bench Test | Safety-critical |
| JSEA-PRO-MET-205-016 | SWI-PRO-MET-205-016 | Precipitate and Platelet Content Determination | Operating |
| JSEA-PRO-MET-205-017 | SWI-PRO-MET-205-017 | Preparation of Standard and Working Solutions | Safety-critical |
| JSEA-PRO-MET-205-018 | SWI-PRO-MET-205-018 | Automatic Titrator Operation and Method Set-Up | Operating |
| JSEA-PRO-MET-205-019 | SWI-PRO-MET-205-019 | Automatic Titrator Electrode Care, Standardisation and Verification | Operating |

6.3  Schedule

| Task | Frequency |
| --- | --- |
| 205-001 Free Cyanide Titration - Silver Nitrate Method | Every shift on every cyanide-bearing stream on the schedule. |
| 205-002 Caustic Soda Strength Titration | Every made-up batch and once per shift on standing solution. |
| 205-003 Sulphuric Acid Strength Titration | Every made-up batch and once per shift on standing solution. |
| 205-004 Sodium Chloride (Chloride) Titration | Every made-up batch and per the analysis schedule. |
| 205-005 Lime Availability Test | Every delivery and weekly on the slaked slurry. |
| 205-006 Lime Addition and Lime Demand Test | On each new ore type and whenever plant lime consumption moves. |
| 205-007 Bottle Roll Leach Test - As-Received and Pulverised | On each new ore type, and on any tail sample being investigated. |
| 205-008 Extended and Diagnostic Leach Test | On tail investigation and on each new ore type. |
| 205-009 CIL/CIP Sequential Triple Contact Testwork | On each new ore type and when adsorption performance is being investigated. |
| 205-010 Carbon Adsorption Capacity and Isotherm Test | Monthly, and on every new carbon delivery. |
| 205-011 Carbon Activity and Ball-Pan Hardness Test | Monthly, and on every new carbon delivery. |
| 205-012 Resin Adsorption Capacity and Kinetics Test | To be set once the vendor data arrives. |
| 205-013 Resin Elution Efficiency and Barren Resin Loading Test | To be set once the vendor data arrives. |
| 205-014 Resin Fouling, Osmotic Shock and Bead Integrity Assessment | Monthly, and after any osmotic shock event. |
| 205-015 Cyanide Destruction (Detox) Bench Test | To be set once the route is chosen. |
| 205-016 Precipitate and Platelet Content Determination | Every lot and per the analysis schedule. |
| 205-017 Preparation of Standard and Working Solutions | As the solution register requires; standards re-standardised at the set interval. |
| 205-018 Automatic Titrator Operation and Method Set-Up | At set-up, and whenever a method is added or changed. |
| 205-019 Automatic Titrator Electrode Care, Standardisation and Verification | Daily standardisation; weekly verification; replacement on failure. |

# 7  FLOWCHART

Not reproduced here. Each work instruction carries its own step sequence in Section 6.

# 8  TRAINING

Every person carrying out a task in this area is trained and signed off against the work instruction for that task, and has signed on to the matching JSEA at a communication session.

- Site induction, current.

- Cyanide awareness and gas detection competency where the area requires it.

- Working at height competency where the task requires it.

- Competency in the determinations, instruments and calculations used in the task.

- Refresher at the interval set by the site training matrix, and after any change to the instruction.

# 9  REFERENCE

- KBK-MIR-MP-PRO-OPE-SOP-0010 Titrasi Sianida

- KBK-MIR-MP-PRO-MET-SOP-0037 Titrasi Sianida dengan Perak Nitrat and SOP-0043 AgNO3 0.01 M standard, both received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0009 Titrasi Kaustik Soda

- KBK-MIR-MP-PRO-MET-SOP-0025 and SOP-0039/0040 hydrochloric acid titration, received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0041 Titrasi Asam Sulfat volume per volume for purity and SOP-0042 weight per volume, both received 11 Aug 2026

- ILS quotation Q0023979 - Hanna HI902C automatic titrator

- ILS quotation Q0023979 - HI902C with ISE channel

- KBK titration method set

- KBK-MIR-MP-PRO-OPE-SOP-0024 Uji Kandungan Kapur

- 4034-046-VE-019 Transmin quicklime slaking plant functional description, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0002 Uji Penambahan Kapur

- KBK-MIR-MP-PRO-OPE-SOP-0003 Uji Pelindian Menggunakan Bottle Roll

- ILS quotation Q0023979 - Bottle Roller MkII 12-place with guarding

- KBK-MIR-MP-PRO-OPE-SOP-0011 Extended Leaching Untuk Leach dan CIL Tail

- KBK-MIR-MP-PRO-MET-SOP-0038 Uji Tail Diagnostik Menggunakan Leachwell, received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0021 CIL Testwork Sequential Triple Contact

- KBK-MIR-MP-PRO-OPE-SOP-0007 Pengujian Kapasitas Adsorpsi Karbon

- KBK-MIR-MP-PRO-MET-SOP-0018 Uji Ekuilibrium Karbon, received 11 Aug 2026 - the equilibrium and isotherm half

- KBK-MIR-MP-PRO-OPE-SOP-0005 Uji Kekerasan Ball-Pan Karbon Aktif

- KBK-MIR-MP-PRO-MET-SOP-0026 Uji Aktifitas Karbon Dengan K[Ag(CN)2], received 11 Aug 2026 - the activity half, which SOP-0005 does not cover

- KBK SOP-PROC-CNREC-01 and -12, received 11 Aug 2026 - operating loading and conditioning practice

- No Goldquip resin performance data held

- KBK SOP-PROC-CNREC-02 Cyanide elution and CNREC-05 Metal elution, received 11 Aug 2026 - operating elution conditions from a working plant, usable as the test target

- No Goldquip resin elution performance data held

- KBK-MIR-MP-PRO-MET-SOP-0058 Distribusi Ukuran Partikel Resin, received 11 Aug 2026

- ILS quotation Q0023979 - 38 um to 2 mm sieve set and Ro-Tap RX29

- RA-01 Resin Loss Register Rev A

- OR-07 Back-up Detox definition memo - the decision is open

- KBK-MIR-MP-PRO-OPE-SOP-0001 Platelet Content

- KBK-MIR-LAB-WET-SOP-043, -044 and -045 standard solutions

- KBK-MIR-MP-PRO-MET-SOP-0043 AgNO3 0.01 M standard, SOP-0050 phenolphthalein indicator, SOP-0051 rhodanine indicator, SOP-0052 10 per cent sulfamic acid and SOP-0053 potassium chloride for the cyanide analyser - all received 11 Aug 2026

- ILS quotation Q0023979 - Class F1 weight set 10 mg to 200 g and GR-200 0.1 mg balance

- ILS quotation Q0023979 - Hanna HI902C automatic titrator with ISE

- KBK-MIR-MP-PRO-MET-SOP-0025, -0037, -0039, -0040, -0041, -0042 and -0043 - the seven titration methods to port, all received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0030 Kalibrasi DO-meter and SOP-0031 Kalibrasi pH-meter, both received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0043 AgNO3 standard, received 11 Aug 2026

- ILS quotation Q0023979

# 10  REVIEW

This procedure and the documents beneath it are reviewed every 12 months, and immediately after any incident, plant change, equipment change or change to the schedule.

# 11  REGISTER TRACEABILITY

The three-digit suffix is shared between the two registers, so SWI-PRO-MET-205-011 is the work instruction for JSEA-PRO-MET-205-011.

Registers: HM-MMM-WHS-REG-JSEA-PRO-updated_10.xlsx tab JSEA_MET, and HM-MMM-WHS-REG-XXX-R00-SWI-SWMS.xlsx tab SWI-MET. GGT working masters are MM-4034-033-OR-03-JSEA-Register-RevE.xlsx and MM-4034-033-OR-03-SWI-Register-RevE.xlsx.

| Item | Count |
| --- | --- |
| Register lines in area 205 | 19 |
| Hazard analyses issued | 19 |
| Work instructions issued | 19 |
| Desk-based tasks with a JSEA but no work instruction | 0 |
| Safety-critical | 7 |
| Issued but NOT FOR USE | 3 |