Safe Work Instruction

Thickener Performance Survey - Flux, Bed Level and Flocculant Response

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots with sound tread - nitrile PVC boots at the sample point

- Chemical resistant suit, nitrile rubber gloves and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-203-007 - Thickener Performance Survey - Flux, Bed Level and Flocculant Response |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-203-007 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Measure what the thickeners are actually doing - solids flux, bed level behaviour, underflow density and how they respond to flocculant. A thickener that is not making underflow density costs water, and one that is losing solids to overflow costs metal and puts solids into process water. Area: 203 Plant Surveys. Points and equipment covered: 051-TH-006 - Tails thickener 071 - Copper precipitate thickener 106 - Flocculant plants, Model 01 and Model 05 Frequency: Quarterly, and whenever overflow clarity or underflow density moves. This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO207 - Plant Surveys and Circuit Performance Assessment. Read that procedure before carrying out this task for the first time. Register line: SWI-PRO-MET-203-007 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-203-007. This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Splash of cyanide-bearing slurry or solution to skin or eyes — Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. Fall from a tank top, launder platform, column platform or access ladder — Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. Contact with an agitator, sample cutter, pump or screen that starts without warning — Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. Slip, trip or fall on wet or slurry-covered walkways around sample points — Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. Manual handling injury from carrying sample buckets, containers and composite drums — Sample volume kept to the schedule - no over-filling. Two-person lift or a trolley for composite containers above the site manual handling limit. Route cleared before lifting. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-203-007 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Working alone in a cyanide area - Gas monitor or fixed detection not healthy - Safety shower or eyewash not proven flowing - Thickener not at steady state |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-203-007 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Confirm a second person is in the area. Cyanide-area work is not done alone. - Notify the control room that the task is starting, and where you will be. - Confirm the personal gas monitor is on, in calibration date and reading clean. - Confirm the safety shower and eyewash nearest the work are within reach and proven flowing. - Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress. Equipment Required : - Sampling buckets - Marcy scale - TSS meter or filter set - Settling cylinders - Stopwatch - Field data sheets - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Steady-State Record and Sampling - HCN released at the open sample point - Splash of cyanide-bearing slurry - Fall from the launder platform - Samples not taken at the same moment |  | - Record the thickener at steady state - feed rate, feed density, bed level, rake torque, underflow rate and flocculant dose. - Sample feed, overflow and underflow simultaneously. - Determine feed and underflow density on the Marcy scale and overflow suspended solids. CAUTION: Open the sample valve slowly, with the container positioned first and the body out of the spray path. Never open a valve whose discharge cannot be seen. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Solids Flux - Flux compared with the wrong design value |  | - Calculate solids flux and compare against the design flux from the Roytec control philosophy. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Settling and Flocculant Dose Tests - Dose varied outside the agreed range - Response read before the change has settled |  | - Run a settling test on the feed at the current flocculant dose and at two other doses, and record the settling rate for each. - Vary the flocculant dose within the agreed range and record the overflow clarity response after each change has settled. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Survey Report - Optimum dose reported without data |  | - Report the optimum dose, the achieved flux and any deviation from the vendor design basis. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Spillage left on the ground - Equipment not returned - Control room not told the task is complete |  | - Leave the area clean. Recover spillage to the drain, not to the ground. - Return all equipment to its storage point. - Record what was done, what was found and anything not completed. - Notify the control room that the task is complete. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| HM-PRC-VXX-PRO207 | Plant Surveys and Circuit Performance Assessment |
| JSEA-PRO-MET-203-007 | JSEA — Thickener Performance Survey - Flux, Bed Level and Flocculant Response |
| HM-MMM-WHS-REG-XXX-R00-SWI-SWMS | SWI / SWMS Register — tab SWI-MET |
| Tail Thickener and Cu Thickener Field Operator Procedures | Site procedures |
| 4034-018A-VE-007 and 4034-018A-VE-045 | Roytec tails thickener control philosophy and IOM, received 11 Aug 2026 - rake torque, bed level and underflow density limits |
| 4034-019-VE-006 and 4034-019B-VE-007 | Roytec Model 01 and Model 05 flocculant control philosophies, received 11 Aug 2026 |
| KBK-MIR-MP-PRO-OPE-SOP-0014 | Settling Test |
| HM-PRC-V01-PRO008 and PRO016 | Tails thickener and copper circuit procedures |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Contact with Moving Equipment If a person is caught by or struck by an agitator, rake, pump or sample cutter, hit the nearest emergency stop, call CH19 “EMERGENCY” and call 000. Do not approach the equipment until it is isolated and locked out. 3. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 4. Skin or Eye Contact with Slurry Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 5. Fall from Height Do not move the injured person unless they are in danger. Call CH19 “EMERGENCY”, call 000, and notify the Shift Supervisor. 6. Slip, Fall or Lifting Injury Call CH19 “EMERGENCY”, call 000 if the injury is serious, and notify the Shift Supervisor.