Mt. Morgan SITE WORK INSTRUCTION

Reagent Solution Strength Sampling - NaCN, NaOH, H2SO4, NaCl, Lime and NaSH

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-201-020 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-201-020 |
| Area | 101 to 107 Reagents |
| Parent procedure | HM-PRC-VXX-PRO205 Plant Sampling and Metallurgical Data Collection |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

DRAFT FOR REVIEW. Martabe work instructions 'Sampling Feed, Product and Final Product of Lime Slaker' (DOC-3-MET-PRS-WIN-00059-IE) as Part B and 'Sampling Hydrated Lime' (DOC-3-MET-PRS-WIN-00061-IE) as Part C added to Section 6, both v1.0 issued 25/12/2024. Not approved until reviewed. JSEA JSEA-PRO-MET-201-020 must be updated for the added hazard row.

# 1  TASK AND SCOPE

Confirm every made-up reagent is at the strength the process assumes before it is dosed.

A reagent made up off-strength is dosed at the wrong rate everywhere it is used, and the error is not visible until the circuit drifts.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 101 | Sodium cyanide - solution and briquettes |
| 102 | Sodium hydroxide - diluted |
| 103 | Lime - slaked slurry |
| 104 | Sodium chloride - made-up solution |
| 105 | Sulphuric acid - diluted |
| 107 | Sodium hydrosulphide - as delivered and dosed |

Frequency: Every batch made up, and once per shift on the standing solutions.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO205 - Plant Sampling and Metallurgical Data Collection. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-201-020 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-201-020.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-201-020 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Contact with sulphuric or hydrochloric acid - burn to skin or eyes | Full acid PPE including face shield, acid-resistant gloves, apron and boots. Sample drawn only from the designated sample valve. Add acid to water, never the reverse. Safety shower and eyewash within reach and proven flowing. Spill kit at the point. |
| Contact with sodium hydroxide solution - burn to skin or eyes | Full chemical PPE including face shield and chemical-resistant gloves. Sample drawn slowly from the designated valve. Safety shower and eyewash within reach and proven flowing. |
| Hydrogen sulphide released from sodium hydrosulphide or from an acidified sulphide stream | Personal multi-gas monitor including H2S worn and in calibration date. Area ventilation confirmed running. Two people, one clear. Withdraw upwind on any alarm. No sampling of the NaSH circuit during acid dosing. |
| Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt | Sampling of solid cyanide done only with the full cyanide PPE set including a gas mask with an A2B2E2K2P3 cartridge. Dust suppression and local extraction confirmed running. No dry sweeping. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Slip, trip or fall on wet or slurry-covered walkways around sample points | Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. |
| Manual handling injury from carrying sample buckets, containers and composite drums | Sample volume kept to the schedule - no over-filling. Two-person lift or a trolley for composite containers above the site manual handling limit. Route cleared before lifting. |
| Working alone in a cyanide area where a collapse would not be seen | Cyanide-area sampling is not done alone. Control room notified at the start and end of every round. Radio check-in at the interval set by the Shift Supervisor. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |
| [JSEA to confirm] Lime dust and contact when sampling bagged hydrated lime, and heat and dust at the lime slaker | Hazmat overall, latex gloves, N95 mask, glasses, hard hat and safety boots. Eyewash proven flowing before starting; wash dust from the eyes at once; wash skin with soap under running water. Lime safety data sheet read. Sampler position watched. Forklift moves done only by an authorised operator. No water in the lime feed pocket at the slaker. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-201-020 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Acid-resistant gloves, apron and face shield

- Chemical splash goggles

- Personal multi-gas monitor including H2S, calibrated and in test date

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Confirm the plant is in steady-state operation - normal operation for a minimum of 15 to 20 minutes before sampling. A sample taken during a swing is not representative.

- Notify the control room or DCS operator that the sampling round is starting, and which points it covers.

- Confirm the personal gas monitor is on, in calibration date and reading clean, and that fixed detection in the area is healthy.

- Confirm the safety shower and eyewash nearest the point are within reach and proven flowing.

- Label every container BEFORE sampling - point, date, time and shift.

- Rinse the container, cutter or sieve with process water and then with the stream being sampled. Discard the rinse.

Equipment required:

- Sample bottles 250 mL, one dedicated set per reagent

- pH meter

- Hydrometer or density meter

- Titration set - burette, pipette, conical flask, stand, wash bottle

- Standardised AgNO3 for cyanide; standardised HCl for caustic; standardised NaOH for acid

- Rhodanine and phenolphthalein indicators

- Distilled water

- Personal protective equipment as Section 5, matched to the reagent being sampled

- [M] Sample containers (sampler) kept at the lime slaker, dry plastic bags, scoop, marker, cable ties, forklift (hydrated lime bags), N95 mask, hazmat overall

# 6  STEPS

Part A - Made-up reagent strength sampling

1.  Read the reagent-specific site sampling procedure before starting - the PPE and the approach differ between cyanide, acid, caustic and NaSH.

2.  NEVER use a container that has held a different reagent. Dedicated, labelled containers only.

3.  For sodium cyanide solution, sample only from the designated valve with full cyanide PPE, including the gas mask with A2B2E2K2P3 cartridge available for immediate use.

4.  For sodium cyanide briquettes, sample the solid with the dust controls in place and do not open the sample in an unventilated space.

5.  For sulphuric acid and sodium hydroxide, sample slowly from the designated diluted-solution valve, never from the concentrated storage tank.

6.  For sodium hydrosulphide, confirm no acid dosing is running anywhere that could contact the stream, and wear the multi-gas monitor including H2S.

7.  Titrate or measure density in the field where the method allows, and bottle the laboratory split for confirmation.

8.  Record batch number, make-up time, measured strength and the target strength against each sample. Report any batch outside the target range to the Shift Supervisor before it is dosed.

Part B - Lime slaker feed, product and final product sampling [M]

[M] = taken from the Martabe team work instruction "Sampling Feed, Product and Final Product of Lime Slaker (DOC-3-MET-PRS-WIN-00059-IE)" (25/12/2024). [CONFIRM] = unspecified or inconsistent in the source; resolve before this instruction is approved for use. Part A (original steps) is unchanged.

[CONFIRM] the source names the Martabe lime slaker feed hopper, product hopper and lime tank. Map these to the Transmin slaking plant points here. The source gives no test to run on the samples and does not say how hot the slurry is, so confirm the bag type and the laboratory request.

9.  Take 5 minutes before starting ('Take 5'). Check the plastic bags are not damaged or leaking [M].

10.  Feed: the sampling point is the feed hopper. Use the sampler kept near the lime slaker. Put the sampler into the feed bin and fill it. Take it out of the bin. Make sure the bag is dry (change a wet bag for a dry one). Put the sample in the bag and tie it tightly.

11.  Product: the sampling point is the product hopper. Open the product bin cover, put the sampler in and fill it, lift it out. Use a dry bag, put the sample in and tie it tightly. Close the product bin cover.

12.  Final product: the sampling point is the lime tank. Put the sampler into the final product bin, fill it, lift it out. Use a dry bag, put the sample in and tie it tightly.

13.  Hazards in the source: dust, contact with the product, the sampler hitting the head, and heat from the lime slurry. Hard hat on; make sure there is no water in the lime feed pocket.

Part C - Bagged hydrated lime sampling [M]

[M] = taken from the Martabe team work instruction "Sampling Hydrated Lime (DOC-3-MET-PRS-WIN-00061-IE)" (25/12/2024). [CONFIRM] = unspecified or inconsistent in the source; resolve before this instruction is approved for use. Part A (original steps) is unchanged.

14.  Check the nearest eyewash works. Prepare plastic bags, marker and scoop. Have the lime safety data sheet available [M].

15.  Bring the sample bag down with the forklift as the forklift operation instruction requires. Only an authorised forklift operator does this.

16.  Write the ID number on the plastic bag. Untie the sample bag and level the surface of the opened lime bag so lime does not spill.

17.  Take the sample with a scoop, spread evenly so the sample is homogeneous across the bag. Take it at least 10 cm below the surface.

18.  Put the sample in the labelled plastic bag. Twist the bag tightly and tie it by hand so no air is left inside. Also tie it with a cable tie. Double-bag it and tie the outer bag the same way.

19.  Close the sample container again. Send the sample and the dispatch form to the laboratory (the source says ITS).

20.  Record the per cent solids of the hydrated lime in 'G:\Processing\5. Metallurgy\Metallurgy Lab\04 Metlab Data\Lime\% Solid Hydrated Lime'. [CONFIRM] a per cent solids result on dry hydrated lime is unusual; confirm the test (lime availability is in SWI-PRO-MET-205-005).

# 7  ON COMPLETION

- Close the sample valve or stop the sample pump and confirm the point is not weeping.

- Wash down the point and the surrounding walkway. Leave nothing on the grating.

- Record sampling time, operator name and the operating conditions read at the time - flow, density and any instrument value available.

- Deliver the labelled samples to the laboratory or to the composite station as the schedule requires, and sign the handover.

- Notify the control room that the round is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- Mt. Morgan site procedures 19. Sodium Cyanide Solution, 20. Sodium Cyanide Briquettes, 21. Diluted Sulphuric Acid and 22. Diluted Sodium Hydroxide Sampling [LIVE]

- KBK-MIR-MP-PRO-MET-SOP-0009 caustic soda titration, SOP-0010 cyanide titration, SOP-0025 and SOP-0039/0040 hydrochloric acid titration, SOP-0041/0042 sulphuric acid titration and SOP-0043 AgNO3 standard preparation - the last six received 11 Aug 2026

- KBK-MIR-MP-PRO-OPE-SOP-0076 Fasilitas Cyanide, received 11 Aug 2026

- 4034-046-VE-019 Rev A Transmin quicklime slaking plant functional description, received 11 Aug 2026

- HM-PRC-V01-PRO021 to PRO027

- Martabe work instruction 'Sampling Feed, Product and Final Product of Lime Slaker' DOC-3-MET-PRS-WIN-00059-IE v1.0 (issued 25/12/2024) - Part B source

- Martabe work instruction 'Sampling Hydrated Lime' DOC-3-MET-PRS-WIN-00061-IE v1.0 (issued 25/12/2024) - Part C source