Safe Work Instruction

Screen and Cyclone Performance Survey - Size Split Determination

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet, safety glasses and hearing protection (double at the mill)

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots with sound tread - nitrile PVC boots at the sample point

- Chemical resistant suit, nitrile rubber gloves and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-203-003 - Screen and Cyclone Performance Survey - Size Split Determination |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-203-003 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Determine the actual size split across each screen and cyclone against what the design assumes. A screen or cyclone not doing what the flowsheet says it does moves the problem downstream, usually into the mill or the adsorption circuit. Area: 203 Plant Surveys. Points and equipment covered: 021-SC-001 - Trash screen 032-SC-002/003 - Loaded carbon and carbon safety screens 041 / 051 - Adsorption interstage and recovery screens Cyclones - overflow and underflow Frequency: Quarterly, and after any panel change or aperture change. This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Splash of cyanide-bearing slurry or solution to skin or eyes — Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. Fall from a tank top, launder platform, column platform or access ladder — Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. Contact with an agitator, sample cutter, pump or screen that starts without warning — Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. Hearing damage in the mill, screen, compressor and blower areas — Hearing protection mandatory in signed areas. Double protection at the mill and compressor. Time at the point kept to what the task needs. Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt — Sampling of solid cyanide done only with the full cyanide PPE set including a gas mask with an A2B2E2K2P3 cartridge. Dust suppression and local extraction confirmed running. No dry sweeping. Slip, trip or fall on wet or slurry-covered walkways around sample points — Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-203-003 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Working alone in a cyanide area - Gas monitor or fixed detection not healthy - Safety shower or eyewash not proven flowing - Hearing damage in the mill and screen areas |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-203-003 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Confirm a second person is in the area. Cyanide-area work is not done alone. - Wear hearing protection in signed areas, with double protection at the mill and compressor. - Notify the control room that the task is starting, and where you will be. - Confirm the personal gas monitor is on, in calibration date and reading clean. - Confirm the safety shower and eyewash nearest the work are within reach and proven flowing. - Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress. Equipment Required : - Sieve set and Ro-Tap shaker - Filter press and filter paper - Drying oven - Balance - Sample containers by stream - Field data sheets - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Simultaneous Sampling - HCN released at the open sample point - Splash of cyanide-bearing slurry - Fall from height at the screen or cyclone - Streams not sampled at the same time |  | - Sample feed, oversize and undersize on the screen, or feed, overflow and underflow on the cyclone, at the same time. - Take increments across the full width or the full discharge, not one grab from the near end. CAUTION: Open the sample valve slowly, with the container positioned first and the body out of the spray path. Hearing protection is mandatory in signed areas. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Filtering, Drying and Weighing - Splash of cyanide-bearing filtrate - Streams mixed up |  | - Filter, dry and weigh each stream. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Sizing - Sieves not cleaned between streams - Mass retained not recorded on every aperture |  | - Screen each to the full sieve set and record the mass retained on each aperture. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Partition Curve and Report - Cut size not compared with the aperture - Torn or wrong panel not reported |  | - Calculate the partition curve and the actual cut size. - Compare the cut size against the stated aperture for the screen, and against the design cut for the cyclone. - Report any screen where the cut size and the aperture do not agree - it usually means a torn or wrong panel. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Spillage left on the ground - Equipment not returned - Control room not told the task is complete |  | - Leave the area clean. Recover spillage to the drain, not to the ground. - Return all equipment to its storage point. - Record what was done, what was found and anything not completed. - Notify the control room that the task is complete. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| JSEA-PRO-MET-203-003 | JSEA — Screen and Cyclone Performance Survey - Size Split Determination |
| KBK-MIR-MP-PRO-OPE-SOP-0008 | Cyclone Efficiency |
| KBK-MIR-MP-PRO-MET-SOP-0029 and SOP-0020 | Sizing Harian COF and Distribusi Logam dan Ukuran, received 11 Aug 2026 |
| MM-4034-033 | Screen Aperture Register |
| 4034-004-VE-025 and 4034-011-VE-022 | Goldquip screen manuals, received 11 Aug 2026 |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Contact with Moving Equipment If a person is caught by or struck by a screen, pump or sample cutter, hit the nearest emergency stop, call CH19 “EMERGENCY” and call 000. Do not approach the equipment until it is isolated and locked out. 3. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 4. Skin or Eye Contact with Slurry Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 5. Fall from Height Do not move the injured person unless they are in danger. Call CH19 “EMERGENCY”, call 000, and notify the Shift Supervisor. 6. Slip, Fall or Lifting Injury Call CH19 “EMERGENCY”, call 000 if the injury is serious, and notify the Shift Supervisor.