Safe Work Instruction

Flocculant Screening and Dose Optimisation Test

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots - nitrile PVC boots

- Chemical resistant suit, nitrile rubber gloves and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-204-010 - Flocculant Screening and Dose Optimisation Test |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-204-010 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Compare flocculant types and doses to find the cheapest one that does the job. Flocculant is a significant consumable and the wrong grade costs both money and thickener performance. Find the settling time at each flocculant solution strength (Step 4), set up the effective treatment dosage test (Step 5), and run the flocculant sieve test on tailing (Steps 6 and 7). Area: 204 Met Lab - Physical Testwork. Points and equipment covered: Met lab bench - physical testwork bench and instrument Frequency: On each new ore type and when a flocculant change is proposed. Draft for review: Steps 4 to 8 are taken from the Martabe work instructions Settling Test with Variance %Strength Flocc (22/03/2025), Effective Treatment Dosage (DOC-3-MET-PMC-WIN-00122-IE) and Flocculant Testwork on Tailing Using Sieve (DOC-3-MET-PMC-WIN-00124-IE), v1.0, 25/12/2024. They are approved for inclusion. Settling cylinders are not purchased; plain 1 L graduated cylinders are approved for use until they are. JSEA-PRO-MET-204-010 must be updated for the added hazards before this instruction is approved. Open items: (1) how the 4 strengths and 4 doses are laid out across the 4 cylinders of a set (Step 4); (2) the basis for 276 g and 12 samples (Step 5); (3) name the Mt. Morgan tailing sample point and the cyanide-bearing return point that replace the Martabe safety carbon screen distributor door and pump PU-372 (see SWI-PRO-MET-201-008); (4) flocculant mixing and ageing time are not stated - Step 2 requires the same ageing for every candidate; (5) bucket size, 10 L or 20 L; (6) the Martabe flocculant make-up SOP is not received; (7) the source reads the settling times as 60, 24 hours, 48 hours - minute 60 is assumed (Step 4); (8) confirm the record folders and forms exist at Mt. Morgan. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Splash of cyanide-bearing slurry or solution to skin or eyes — Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Cuts from broken glassware, and burns from hot glassware — Glassware inspected for chips and cracks before use and discarded if damaged. Hot glassware handled with tongs or heat-resistant gloves and set down on a heat mat. Broken glass to the sharps bin, never to the general waste or by hand. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. [JSEA to confirm] Solution splash and spill, and a pinch point on the level gauge — Latex gloves, glasses and safety boots. Eyewash proven flowing and spill kit at hand; wash splashes under running water; clean spills at once. Keep hands clear of the level gauge pinch point. [JSEA to confirm] Acetone (flammable), sieve and caliper pinch points, stairs, and uneven or slippery surfaces — Acetone safety data sheet read; glasses on; no smoking or flame; clean spills on clothing with plenty of water. Keep hands clear of sieve and caliper pinch points. Three points of contact and chains and handrails in place on stairs. Good housekeeping and care on rough or wet ground. Dust mask; eyewash proven flowing; wash contact with soap under running water. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-204-010 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Fume cupboard or scrubber not running - Safety shower or eyewash not proven flowing - Instrument out of calibration |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-204-010 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Take 5 and prepare the sampling equipment, cylinders, balance, syringes, beakers, sieve and pan, measuring cylinders, turbidity meter, camera, ruler, calipers, stopwatch and clip bags. Make sure the acetone is in date. - Confirm settling cylinders and a flocculant test rig are available before planning the test. Until settling cylinders are purchased, use 1 L graduated cylinders. - Confirm the fume cupboard airflow, the scrubber and its dosing are running before any acid or cyanide work at the bench. - Confirm the safety shower and eyewash are within reach and proven flowing. - Confirm the instrument or balance is within its calibration or verification interval. - Confirm the reagents to be used are in date and correctly labelled. - Inspect all glassware for chips and cracks and discard anything damaged. Equipment Required : - Settling cylinders - NOT PURCHASED; 1 L graduated cylinders used until they are - Flocculant samples from candidate suppliers - Stopwatch - Pipettes - Plunger - Balance, syringe, beakers, 250 mL sample bottles, vertical stirrer, filter press, drying oven - Laboratory flocculant, process water, acetone; slurry characterisation spreadsheet (density to per cent solids) - Level gauge, sieve, turbidity meter with cuvettes, cone, bucket, iron stirrer - 2 m dip sampler, lab sample shovel, bucket, 1.18 mm sieve with pan, cylinder, 500 mL and 120 mL measuring cylinders, camera, ruler, calipers, clip sample bags - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Flocculant Make-up and Shortlist - Candidates made up at different strengths - Flocculant solution splash and spill |  | - Make up each candidate flocculant at the same strength and ageing time. - Run the settling test at a fixed dose across all candidates first, to shortlist. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Dose Response and Costing - Cuts from a broken cylinder - Result not related to the plant basis |  | - Run the dose response on the shortlist. - Record settling rate, overflow clarity and underflow density for each. - Cost each option per tonne treated at its optimum dose. - Report against the plant flocculant basis in the Roytec control philosophies. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Settling Test with Solution Strength Variance - Cylinder weights not matched - Wrong flocculant volume added - Splash of cyanide-bearing tailing |  | - Make up flocculant solutions at 0.35, 0.40, 0.45 and 0.50 per cent with process water. - Stir the tailing sample until even with the vertical stirrer. - Put 1 L of tailing slurry in a graduated cylinder and weigh it. Prepare 4 cylinders for one test set. - Check the weight difference between cylinders is below 4 g. If it is above 4 g, stir again and repeat the previous step. - Open the slurry characterisation spreadsheet. Enter ore density 2.6 t/m3. Enter the 1 L slurry weight as pulp density (RHOP): 1.5 kg per litre is entered as 1.5 (1.5 kg/L = 1.5 t/m3). Read off solids mass and per cent solids. - Record the solution strength and the dose. - Flocculant volume (mL) = dose (g/t) x slurry mass (g) x per cent solids / (solution strength in per cent x 1,000,000). The source writes this as 100 x solids mass (g) / 1,000,000 x 100 / 0.5, where 100 and 0.5 are an example dose of 100 g/t and a 0.5 per cent solution; use the actual dose and strength for each cylinder. - Add flocculant at doses of 70, 80, 90 and 100 g/t. - Mix the sample with the stirring rod 8 times. - Record the solids level at minute 5, 10, 15, 30, 60 and at 24 hours and 48 hours. - Separate the solids from the water with the filter press. - Dry the sample in the oven and weigh it dry to correct the dose to g/t. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Effective Treatment Dosage (ETD) Test - Solids settling in the bucket - Pinch point on the level gauge - Turbidity read on a dirty cuvette |  | - Have the flocculant and the slurry sample ready. - Stir the slurry in the bucket with the iron stirrer so no solids settle. - While stirring, take slurry and weigh 276 g into a beaker. Repeat 12 times to get 12 samples. - Carry out the flocculant test as in Step 7. - Check the turbidity of the water that came through the sieve: power on the turbidity meter, put the cuvette in the sample holder, press read, wait for the result and record it. Take the cuvette out. - Record the ETD data in G:\\Processing\\5. Metallurgy\\Metallurgy Lab\\04 Metlab Data\\ETD & Settling Test or on form DOC-4-MET-PMC-DFR-00140-EN (Form ETD Data.xlsx). CAUTION: Keep hands clear of the level gauge pinch point. Clean spills at once. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Tailing and Flocculant Sampling for the Sieve Test - HCN at the tailing sampling point - Stairs and uneven or slippery ground - Acetone is flammable |  | - Tailing: use the dip sampler with the 2 m handle at the tailing sample point (to be confirmed). Lower the sampler until slurry fills the cylinder. - Pour into the Marcy scale tube and measure per cent solids. The Marcy scale must be calibrated per the per cent solids procedure. Record the per cent solids. - Fill a bucket with tailing sample. - Flocculant from the bag: sample from one stack of bags only. Untie the top of the bag and use the lab shovel to take 5 to 10 g into a clip bag. Retie the bag. - Dilution: weigh the flocculant to the strength the metallurgist asks for (0.5 per cent means 0.5 g). Add 3 mL acetone, then 97 mL water to make 100 mL. CAUTION: The tailing slurry is cyanide-bearing. Apply the cyanide controls of SWI-PRO-MET-201-008 and 201-017 and keep the personal HCN monitor on at the sampling point. Keep acetone away from flame and smoking. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Flocculant Sieve Testwork - Pinch points at the sieve and calipers - Splash of cyanide-bearing slurry - Dose calculated wrongly |  | - Put a 500 mL beaker on the balance and tare. Stir the tailing slurry, pour 300 mL into the beaker and weigh it. - Flocculant volume (mL) = dose (g/t) x slurry mass (g) x per cent solids / (solution strength in per cent x 1,000,000). Example: 60 g/t, 400 g slurry, 46 per cent solids, 0.4 per cent strength: 60 x 400 x 46 / 400,000 = 2.76 mL. - Draw the flocculant into a syringe and add it to the slurry in the beaker. - Pour the slurry into a second beaker and back into the first, 8 pours in all. - Wait 2 minutes, then pour slowly into the cylinder standing on the 1.18 mm screen. The water drains first into the pan under the screen. - Wait 2 minutes, lift the cylinder slowly and measure the height of the slump with the calipers. - Lift the 1.18 mm sieve. Photograph the slump on the sieve and in the pan from the side and the front, with the date, name and type of flocculant, solution strength and dose. - Tilt the lower tray. Draw the surface water with a syringe into the measuring cylinder and record the volume. - Filter the solids on the sieve and in the pan separately on different filter papers, labelled sieve and pan. Pour the liquid into the bucket. - Dry the solids and weigh them. - Repeat for 30, 40, 60, 80 and 120 g/t, or as the metallurgist instructs. - Record the results in G:\\Processing\\5. Metallurgy\\Metallurgy Lab\\04 Metlab Data\\ETD & Settling Test or on form DOC-4-MET-PMC-DFR-00146-EN (Form Settling Test calc.xlsx). CAUTION: Keep hands clear of the sieve and caliper pinch points. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Waste Return - Cyanide-bearing waste to the wrong drain |  | - Return all leftover flocculant, slurry and wash water to the plant. Take the bucket to the cyanide-bearing return point (to be confirmed) and pour it near the pump. Clean the bucket with process water in the plant. CAUTION: Tailing slurry and wash water are cyanide-bearing. They do NOT go to the general drain. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Cyanide-bearing residue to the general drain - Glassware left dirty - Result not traceable to the instrument |  | - Wash down the bench and the fume cupboard working surface. - Clean glassware and return it to the drying rack. - Dispose of residues to the correct waste stream - cyanide-bearing effluent does NOT go to the general drain. - Record the result, the method used and the instrument or balance identity. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| JSEA-PRO-MET-204-010 | JSEA — Flocculant Screening and Dose Optimisation Test |
| 4034-019-VE-006 and 4034-019B-VE-007 | Roytec Model 01 and Model 05 flocculant plant control philosophies, received 11 Aug 2026 - the plant make-up concentration and dose basis |
| Settling Test with Variance %Strength Flocc (22/03/2025) | Martabe WI (Indonesian) - source of Step 4 |
| DOC-3-MET-PMC-WIN-00122-IE v1.0 | Martabe WI Effective Treatment Dosage (25/12/2024) - source of Step 5 |
| DOC-3-MET-PMC-WIN-00124-IE v1.0 | Martabe WI Flocculant Testwork on Tailing Using Sieve (25/12/2024) - source of Steps 6 to 8 |
| DOC-IV-MET-CHH-SOP-00039 | Martabe SOP referenced by the Martabe WIs - not received |
| DOC-4-MET-PMC-DFR-00140-EN and 00146-EN | Form ETD Data and Form Settling Test calc |
| SWI-PRO-MET-201-008 and 201-017 | Cyanide controls at the tailing and thickener sampling points |
| SWI-PRO-MET-201-020 | Flocculant solution sampling (reagent area) |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 3. Skin or Eye Contact with Slurry Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 4. Cuts from Broken Glassware Apply pressure to stop the bleeding, get a trained first aider, and report to the Shift Supervisor. Call CH19 “EMERGENCY” and 000 for a serious cut. 5. Slip, Fall or Lifting Injury Call CH19 “EMERGENCY”, call 000 if the injury is serious, and notify the Shift Supervisor.