Safe Work Instruction

Lime Addition and Lime Demand Test

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots - nitrile PVC boots

- Chemical resistant suit, acid-resistant and nitrile rubber gloves, and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-205-006 - Lime Addition and Lime Demand Test |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-205-006 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Determine how much lime the ore actually needs to hold the target pH through the leach. Lime demand varies with ore. Dosing to a fixed rate rather than to demand either wastes lime or loses pH control, and losing pH control in a cyanide circuit releases HCN. A second method compares neutralisation reagents on acid water - hydrated lime, quicklime or caustic, with or without air and hydrogen peroxide - on samples confirmed free of cyanide. Area: 205 Met Lab - Chemical and Leach Testwork. Points and equipment covered: Met lab bench - physical testwork bench and instrument Acid water samples - neutralisation testwork, cyanide-free samples only Frequency: On each new ore type and whenever plant lime consumption moves; neutralisation tests when the metallurgist requests them. Draft for review: Steps 4 to 7 combine the Martabe work instructions Dosing NaOH vs Ca(OH)2 to pH 6, 7, 8 and 9, MHR1 Quick Lime Metal Removed, MHR1 Quick Lime and Caustic (V1 and V1.2) and TSF Toe to WPP Test (moved from SWI-PRO-MET-205-015) into one acid water neutralisation method. The Martabe sample names (SP09, MHR-1, TSF Toe) and the numbers in the Martabe record tables are not used. JSEA-PRO-MET-205-006 must be updated for the added hazards before this instruction is approved. Open items: (1) name the Mt. Morgan acid water streams this test is run on, and their sample points; (2) set the air flow and the way the air is added; (3) set the hydrogen peroxide strength and the dose per litre of sample; (4) confirm the assay laboratory and analyte suite for each water; (5) the Martabe tables report solid reagent in mL/L - report in g/L or kg/m3. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Contact with sodium hydroxide solution - burn to skin or eyes — Full chemical PPE including face shield and chemical-resistant gloves. Sample drawn slowly from the designated valve. Safety shower and eyewash within reach and proven flowing. Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt — Sampling of solid cyanide done only with the full cyanide PPE set including a gas mask with an A2B2E2K2P3 cartridge. Dust suppression and local extraction confirmed running. No dry sweeping. Splash of cyanide-bearing slurry or solution to skin or eyes — Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. Cuts from broken glassware, and burns from hot glassware — Glassware inspected for chips and cracks before use and discarded if damaged. Hot glassware handled with tongs or heat-resistant gloves and set down on a heat mat. Broken glass to the sharps bin, never to the general waste or by hand. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. [JSEA to confirm] Lowering or holding sample pH below 10.5 on a sample that contains cyanide - HCN release — Part B is run only on samples confirmed cyanide-free before the test starts. Any cyanide present: stop, do not add reagent, report to the Shift Supervisor. Part A and all cyanide work keep the pH above 10.5 rule. [JSEA to confirm] Quicklime slaking in the sample and hydrogen peroxide contact — Quicklime added in small increments to the stirred sample - slaking heats the slurry and can spit. Avoid dust. Face shield, chemical splash goggles and chemical-resistant gloves (the source lists only safety glasses and rubber gloves, which is below Section 4). Hydrogen peroxide handled with the same PPE; fresh solution, no storage in the work area. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-205-006 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Fume cupboard or scrubber not running - Safety shower or eyewash not proven flowing - Instrument out of calibration |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-205-006 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Confirm the fume cupboard airflow, the scrubber and its dosing are running before any acid or cyanide work at the bench. - Confirm the safety shower and eyewash are within reach and proven flowing. - Confirm the instrument or balance is within its calibration or verification interval. - Confirm the reagents to be used are in date and correctly labelled. - Inspect all glassware for chips and cracks and discard anything damaged. Equipment Required : - Bottles or beakers with stirrers - pH meter, calibrated, and TDS meter - Lime slurry at known strength - Pipettes, balance and stopwatch - Jar test stirrer and 500 mL glass beakers - Baffle tanks with agitator or magnetic stirrer - Hydrated lime, quicklime and caustic in weighed doses - Hydrogen peroxide and plant air supply - Filter apparatus, sample bottles and camera - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Lime Demand - Curve to Target pH - HCN if pH control is lost - Lime dust or splash |  | - Prepare the ore slurry at the plant leach density. - Measure and record the natural pH before any addition. - Add lime slurry in measured increments, stirring and allowing the pH to stabilise between additions. - Record pH against cumulative lime added. - Continue past the target pH so the curve shape either side is known. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Lime Demand - Maintenance and Report - Maintenance demand not measured |  | - Hold the slurry at the target pH and record any further lime needed over the leach residence time - that is the demand the plant actually has to meet. - Report the lime addition to reach target and the maintenance demand separately. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Neutralisation Test - Cyanide Check and Set-up - HCN if a cyanide-bearing sample goes below pH 10.5 - Sample not identified |  | - STOP condition: this test takes the sample to pH values below 10.5. Run it only on a sample confirmed free of cyanide (free, WAD and total cyanide). If cyanide is present at any level, do not start - report to the Shift Supervisor. - Record the sample name, its origin and the date (see Open items). - Take a 100 mL feed sample for pH, TDS and base metal assay before any reagent is added. - Put the measured sample volume in each beaker or baffle tank - for example 500 mL per beaker or 1 L per baffle tank - and start the stirrer or agitator. Record the volume in each. - Photograph the initial condition. Measure and record the initial pH and TDS of each sample. CAUTION: Cyanide-free samples only. Below pH 10.5 any cyanide releases HCN. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Neutralisation Test - Reagent Addition - Quicklime slaking heat and spitting - Hydrogen peroxide contact - Target pH overshot |  | - Run one beaker or tank per reagent or option - hydrated lime, quicklime or caustic; and, where the test requires it, with plant air, or with plant air and hydrogen peroxide added at the start (see Open items). - Add the reagent slowly in small weighed doses, for example 0.5 g, while stirring. - After each addition wait for the pH to stabilise, at least 5 minutes, then record the pH, the TDS and the dose. - Use smaller doses once the pH passes about 5.5. A single 0.5 g quicklime dose has taken a sample from pH 6.2 to 9.58. - Continue to each target pH in turn - for example pH 4, 6, 7, 8, 9 and 10, as the test requires. Photograph and record the cumulative dose at each target pH. CAUTION: Quicklime heats as it slakes and can spit - add in small doses. Hydrogen peroxide with face shield and chemical-resistant gloves. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Neutralisation Test - Settling and Assay - Solids handled without PPE - Sample codes mixed up |  | - At each target pH the test calls for, take a 100 mL sample for base metal assay. - At the final pH, let the solids settle. Record the settling time and photograph the sample while settling and when settled, for a maximum of 2 hours. Note whether a precipitate has formed. - Filter. Submit 100 mL of solution and 50 g of solids for assay. Code every sample with the reagent, the run and the pH. - Request the dissolved base metal suite - Al, Cd, Cu, Fe, Mn, Ni, Zn, Cr, Pb, Na, Hg, As, Mg, Ca, SO4, Cl, TSS and TDS - with the final pH, and nitrite, free ammonia, fluoride, COD and BOD where the water requires them. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Neutralisation Test - Records - Consumption in the wrong unit - Martabe numbers carried forward |  | - For each addition record the pH and TDS before, the dose in g, the pH and TDS after, and the cumulative reagent mass. - Report the reagent consumption to each pH in g/L (kg/m3) and compare the reagents at each pH. - Do not carry forward the numbers in the Martabe record tables. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Cyanide-bearing residue to the general drain - Glassware left dirty - Result not traceable to the instrument |  | - Wash down the bench and the fume cupboard working surface. - Clean glassware and return it to the drying rack. - Dispose of residues to the correct waste stream - cyanide-bearing effluent does NOT go to the general drain. - Record the result, the method used and the instrument or balance identity. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| JSEA-PRO-MET-205-006 | JSEA — Lime Addition and Lime Demand Test |
| KBK-MIR-MP-PRO-OPE-SOP-0002 | Uji Penambahan Kapur |
| Martabe WI (undated) | Dosing NaOH vs Ca(OH)2 untuk mencapai pH 6, 7, 8 dan 9 - source of Steps 4 to 7 |
| Martabe WI (undated) | MHR1 sample - Konsumsi Quick Lime Metal Removed (Work_Instruction_MHR_1_Liming_vs_Limingair) - air and peroxide options |
| Martabe WI V1 and V1.2 (undated) | MHR1 sample - Konsumsi Quick Lime dan Caustic - TDS tracking and small doses |
| Martabe WI (undated) | TSF Toe to WPP Test (Work_Instruction_Tsf_Toe) - moved from SWI-PRO-MET-205-015 |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Skin or Eye Contact with Reagent Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 3. HCl Gas or Acid Contact Leave the area upwind. Flush skin or eyes with copious water at the safety shower or eyewash for a minimum of 15 minutes. If breathing is affected call CH19 “EMERGENCY” and call 000. 4. Cuts from Broken Glassware Apply pressure to stop the bleeding, get a trained first aider, and report to the Shift Supervisor. Call CH19 “EMERGENCY” and 000 for a serious cut.