Safe Work Instruction

Resin Adsorption Capacity and Kinetics Test

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots - nitrile PVC boots

- Chemical resistant suit, acid-resistant and nitrile rubber gloves, and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-205-012 - Resin Adsorption Capacity and Kinetics Test |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-205-012 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Measure the loading capacity and adsorption rate of the GG1200M and GG1200C resins. Resin capacity is the design basis of the whole ReCYN circuit. The adsorption rate is measured by the Martabe resin activity test on a cyanide-copper solution and by the fresh resin adsorption test on CIL slurry. Area: 205 Met Lab - Chemical and Leach Testwork. Points and equipment covered: Met lab bench - physical testwork bench and instrument 032-TK-006 - last CIL tank, discharge to ReCYN, slurry for the adsorption test Frequency: To be set once the vendor data arrives. Draft for review - NOT FOR USE until approved. Steps 2 to 6 follow the Martabe work instructions Resin Activity Test (03/03/2025) and Adsorption Test Fresh Resin (09/01/2025). The KCN variant of the activity test is not used. The Martabe CIL tank 7 launder to detox is mapped to the discharge of the last CIL tank (032-TK-006) to ReCYN. JSEA-PRO-MET-205-012 must be updated for the added hazards before this instruction is approved. Open items: (1) acceptance targets for GG1200M and GG1200C need Goldquip resin performance data, not received; (2) loading capacity is not covered by the Martabe method - a capacity method is still needed; (3) confirm the sizing screens (1.18 and 1.4 mm in the source, 0.9 mm in this SWI) against the Goldquip resin specification; (4) the CuSO4 solution strength, and the sample the per cent solids check applies to, are not stated; (5) confirm the values highlighted in the source - 150 mL samples, sample times, filtering and the Cu and Fe assay. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Inhalation of acid fume or reagent vapour at the bench — Work carried out inside the fume cupboard with the sash at the marked working height and the airflow confirmed before starting. Scrubber running and its dosing confirmed. Perchloric work only in the cupboard rated for it, with the washdown routine after every use. No work at an open bench. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. [JSEA to confirm] Weighing and dissolving solid sodium cyanide and caustic; copper-cyanide solution at the bench — Weigh and dissolve inside the fume cupboard with airflow confirmed. Caustic added and pH verified above 10.5 BEFORE any cyanide is added. Full cyanide PPE per Section 4. Not done alone. Copper-cyanide waste to the cyanide-bearing stream only. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-205-012 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Fume cupboard or scrubber not running - Safety shower or eyewash not proven flowing - Instrument out of calibration |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-205-012 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Confirm a second person is in the laboratory for any cyanide work. Cyanide work is not done alone. - Confirm the fume cupboard airflow, the scrubber and its dosing are running before any acid or cyanide work at the bench. - Confirm the safety shower and eyewash are within reach and proven flowing. - Confirm the instrument or balance is within its calibration or verification interval. - Confirm the reagents to be used are in date and correctly labelled. - Inspect all glassware for chips and cracks and discard anything damaged. Equipment Required : - Bottle roller - Agitator with blade and baffle tank (1 L working volume) - Wet-sizing screens 1.18 mm and 1.4 mm, and 0.9 mm screen - Balance, 250 mL sample bottles, filter paper, funnel and stopwatch - Tea strainer and syringe - pH meter - NaCN, CuSO4.5H2O, caustic and distilled water - Fresh, loaded and Cu-eluted resin samples - Solutions at known metal and cyanide concentration - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Resin Sizing - Cyanide-bearing resin handled - Carbon left in the resin |  | - Pan the sample to separate carbon from resin. - Stack the 1.18 mm and 1.4 mm screens and wet-size the sample. - Keep the resin that passes the 1.4 mm screen and is retained on the 1.18 mm screen (see Open items). |  |  |  |  |  |  |  |  |  |  |  |  |
| - Activity Test - Solution - Solid NaCN handling - HCN below pH 10.5 - Copper-cyanide solution |  | - Check per cent solids (see Open items). - Weigh 2 g NaCN inside the fume cupboard. Measure 5 mL CuSO4.5H2O solution. - Put 5 L distilled water in the container and add the 5 mL copper sulphate. - Raise the pH to 10.5 or above with caustic and hold it there. The Martabe range of 10 to 10.5 is not used. - Add the weighed NaCN only when the pH is confirmed at 10.5 or above, and agitate until fully dissolved. - Take a 20 mL head sample. Titrate for NaCN and submit for Cu assay. CAUTION: NEVER add cyanide below pH 10.5. Weigh and dissolve NaCN in the fume cupboard. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Activity Test - Adsorption - Cyanide splash during sampling - Resin lost with the sample |  | - Put 1 L of the prepared solution in the baffle tank and add 5 g of resin sample. - At minute 5, 10, 15, 20 and 30 stop the agitator, take a 20 mL solution sample, separate the resin from the solution and return the resin to the tank. - Titrate each sample for cyanide and send the remaining sample for Cu assay. - Run fresh resin as the reference, then the loaded and Cu-eluted samples. - Record time, initial, sample and final volume, solution pH and NaCN mg/L for every sample. |  |  |  |  |  |  |  |  |  |  |  |  |
| - CIL Slurry Adsorption - Set-up - HCN at the CIL launder - Cyanide-bearing slurry splash |  | - Take 5 L of slurry per resin type from the discharge of the last CIL tank (032-TK-006) to ReCYN, as SWI-PRO-MET-201-004. - Put the 5 L of slurry in the baffle tank in the fume cupboard. Take a 150 mL slurry sample as the 0 minute sample. - Add 10 g of fresh resin (2 g/L) to the baffle tank. CAUTION: Cyanide-bearing slurry. Personal HCN monitor on, fume cupboard, not alone. |  |  |  |  |  |  |  |  |  |  |  |  |
| - CIL Slurry Adsorption - Sampling and Results - Resin sampled with the slurry - Cyanide-bearing filtrate |  | - Take 150 mL samples through a strainer so no resin is sampled, at minute 2, 5, 10, 20, 40 and 60. Record the pH at each time. - Filter the solids from the solution. - Titrate the filtered solution and send the remainder for NaCN titration and Cu and Fe assay. - Enter the results in the logsheet - time, initial slurry volume, sample volume, final volume, remaining solution, solution sample, solution pH and NaCN mg/L. Start from the actual initial volume of 5 L, not the 4000 mL in the Martabe table. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Cyanide-bearing residue to the general drain - Glassware left dirty - Result not traceable to the instrument |  | - Wash down the bench and the fume cupboard working surface. - Clean glassware and return it to the drying rack. - Dispose of residues to the correct waste stream - cyanide-bearing effluent does NOT go to the general drain. - Record the result, the method used and the instrument or balance identity. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| JSEA-PRO-MET-205-012 | JSEA — Resin Adsorption Capacity and Kinetics Test |
| KBK SOP-PROC-CNREC-01 and -12 | Operating loading and conditioning practice (received 11 Aug 2026) |
| Goldquip resin performance data | Not held |
| Martabe WI (03/03/2025) | Resin Activity Test - source of Steps 2 to 4 |
| Martabe WI (09/01/2025) | Adsorption Test Fresh Resin (Work_Instruction_Adsorption_Resin_-_2_gpl) - source of Steps 5 and 6 |
| Martabe WI (undated) | Resin Activity Test KCN and Copper Adsorption (earlier variant) - reference only, not used |
| SWI-PRO-MET-201-004 | CIL Sampling Round - 032-TK-002 to 032-TK-006 Launders |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 3. Skin or Eye Contact with Reagent Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 4. Contact with Moving Equipment If a person is caught by or struck by the agitator, hit the nearest emergency stop, call CH19 “EMERGENCY” and call 000. Do not approach the equipment until it is isolated and locked out. 5. Cuts from Broken Glassware Apply pressure to stop the bleeding, get a trained first aider, and report to the Shift Supervisor. Call CH19 “EMERGENCY” and 000 for a serious cut.