Safe Work Instruction

Resin Elution Efficiency and Barren Resin Loading Test

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots - nitrile PVC boots

- Chemical resistant suit, acid-resistant and nitrile rubber gloves, and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-205-013 - Resin Elution Efficiency and Barren Resin Loading Test |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-205-013 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Measure how completely the elution circuit strips the resin, at the bench. Barren resin loading is to the resin circuit what barren carbon is to the CIL circuit. The bench methods come from the Martabe resin testwork - preconditioning, copper elution, NaCl comparison, eluant scale dissolution, NaCN-NaCl mixing, copper loading by Zn(CN)4 elution, and the dosing pump calibration they use. Area: 205 Met Lab - Chemical and Leach Testwork. Points and equipment covered: Met lab bench - physical testwork bench and instrument Frequency: To be set once the vendor data arrives. Draft for review - NOT FOR USE until approved. Steps 2 to 10 follow the Martabe work instructions Testing NaCl from New Vendor (11/01/2025), Preconditioning Resin with Cu Variance V2 (07/02/2025), Testwork Pelarutan Scaling Eluant Garam Menggunakan Sulfamic Acid (07/10/2025), IPHK Mixing Larutan Campuran NaCN-NaCl (undated), Copper Loading Test (DOC-3-MET-MEL-WIN-00113-IE, 25/01/2025) and Dosing Pump Grundfos DDA Calibration (DOC-3-MET-PMC-WIN-00120-IE, 25/12/2024). Preconditioning follows V2. Every cyanide addition is made at pH 10.5 or above. JSEA-PRO-MET-205-013 must be updated for the added hazards before this instruction is approved. Open items: (1) acceptance targets need Goldquip resin elution data, not received; (2) the NaCN to CuSO4 ratio differs between the NaCl vendor method and V2 (about 0.107 against 0.15 g/mL), and the CuSO4 solution strength and hydrate are not stated; (3) confirm the eluant strength of 29.4 g NaCN in 600 mL (about 49 g/L); (4) confirm which NaCl sources the four resin charges represent; (5) confirm the plant NaCl and NaCN solution strengths for the mixing test, and what IPHK stands for; (6) the source adds the KCN solution to the zinc sulphate solution, which is slightly acidic - confirm the order with HSE; adding the zinc sulphate to the alkaline KCN keeps the cyanide alkaline; (7) confirm the Mt. Morgan cyanide-bearing route for the hi-cyanide eluate - the Martabe tailing sump pump is a source name; (8) confirm the dosing pump hose connections against the pump manual; (9) confirm the Mt. Morgan worksheets for the elution, copper loading and pump calibration records - the Martabe G: drive files and forms are source names. This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Contact with sulphuric or hydrochloric acid - burn to skin or eyes — Full acid PPE including face shield, acid-resistant gloves, apron and boots. Sample drawn only from the designated sample valve. Add acid to water, never the reverse. Safety shower and eyewash within reach and proven flowing. Spill kit at the point. Contact with hot solution or hot surface at the elution, stripping or regeneration circuits — Confirm the circuit is not on a heating cycle before sampling. Heat-resistant gloves and face shield. Allow the sample line to flush and cool before collecting. Do not sample a column under pressure. Inhalation of acid fume or reagent vapour at the bench — Work carried out inside the fume cupboard with the sash at the marked working height and the airflow confirmed before starting. Scrubber running and its dosing confirmed. Perchloric work only in the cupboard rated for it, with the washdown routine after every use. No work at an open bench. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. [JSEA to confirm] Weighing and dissolving solid sodium cyanide for a concentrated eluant, and cyanide-bearing eluate — Weigh and dissolve inside the fume cupboard with airflow confirmed. Caustic added and pH verified above 10.5 BEFORE any cyanide is added. Full cyanide PPE per Section 4. Not done alone. Eluate and rinse to the cyanide-bearing stream only - no general drain. [JSEA to confirm] HCN release when sulfamic acid contacts cyanide-bearing scale — Scale test only in the fume hood with the personal HCN monitor on and the action level of 5 ppm applied: stop, dilute with water, evacuate. Not unattended. Not done alone. Sulfamic acid solution and residue to the cyanide-bearing stream until the scale is shown to be cyanide-free. [JSEA to confirm] Bulk hi-cyanide zinc cyanide eluant (2.2 L, 351 g KCN) mixed at the bench and run for 6 hours — Mixed and run only in the fume hood with the personal HCN monitor on. Caustic and pH above 10.5 confirmed BEFORE any KCN is added; KCN added only to alkaline water. No acid in the work area. Not unattended and not done alone. Bottles labelled 'hi cyanide'. Eluate, drain and rinse to the cyanide-bearing stream only. [JSEA to confirm] Pinch point when fitting the quick-connect hose — Keep hands clear of the pinch point and a safe distance kept; chemical-resistant gloves worn when fitting the quick connect. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-205-013 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Fume cupboard or scrubber not running - Safety shower or eyewash not proven flowing - Instrument out of calibration |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-205-013 at a communication session, site inducted with current cyanide awareness and gas detection competency where the area requires it, and authorised by the Shift Supervisor. - Confirm a second person is in the laboratory for any cyanide work. Cyanide work is not done alone. - Do all cyanide work in this instruction inside the fume cupboard. - Confirm no acid is in the fume cupboard or the work area while any cyanide solution is open. - Take 5 and prepare the equipment, reagents and sample bottles for the test. Check the equipment is in good condition and every reagent is in date. - Confirm the fume cupboard airflow, the scrubber and its dosing are running before any acid or cyanide work at the bench. - Confirm the safety shower and eyewash are within reach and proven flowing. - Confirm the instrument or balance is within its calibration or verification interval. - Confirm the reagents to be used are in date and correctly labelled. - Inspect all glassware for chips and cracks and discard anything damaged. Equipment Required : - Bench elution columns 150 mL and 300 mL, Grundfos DDA dosing pump, quick-connect hose and fittings - Baffle tank with agitator or magnetic stirrer - Balance, beakers 150 and 500 mL, measuring cylinders, sample bottles labelled hi cyanide - pH meter, stopwatch, filter paper, plastic bag for resin sampling - Fresh and loaded resin samples - NaCN, KCN, CuSO4, caustic (solid and solution), NaCl (plant and vendor), zinc sulphate heptahydrate - AgNO3 0.1 M and 0.01 M - Sulfamic acid, eluant salt scale sample, raw and process water - Eluant solutions and heating - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Preconditioning - Copper Loading on Fresh Resin - Solid NaCN handling - HCN below pH 10.5 - Copper-cyanide solution |  | - Put 4 L distilled water in the baffle tank. Adjust and hold the pH at 10.5 to 12 with caustic. - Dose for the copper level under test (V2, 300 mL resin): 70 kg/t = 20.42 g NaCN and 136.4 mL CuSO4 solution; 100 kg/t = 29.17 g and 194.9 mL; 125 kg/t = 36.46 g and 243.6 mL. Add the NaCN and mix, then the CuSO4, keeping the pH at 10.5 to 12. - Sample 100 mL and record the final pH. Titrate with AgNO3 0.01 M and send the remainder for Cu assay as the head. - Put 300 mL of fresh resin in the column and inject the solution for 1 hour at 1 L/h. Flush the column with 200 mL distilled water. - Record the final product volume, stir, and sample 100 mL as the precondition tail. Titrate with AgNO3 0.01 M and send the remainder for Cu assay. - Split the resin - 150 mL for the elution or copper loading test and 150 mL for Cu assay by AAS. For the NaCl comparison prepare four preconditioned resins (see Open items). CAUTION: Raise the pH to 10.5 or above BEFORE any cyanide is added. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Copper Elution Test - Eluant - Concentrated NaCN eluant - HCN below pH 10.5 |  | - Weigh 29.4 g NaCN (see Open items) and 36.2 g NaCl - plant or vendor sample under test. - Put 300 mL distilled water in a beaker, add the NaCl and stir. - Adjust to pH 10.5 to 11 with NaOH. Confirm the pH is 10.5 or above before the NaCN is added. - Add the NaCN and stir. Make up to 600 mL with distilled water and stir. CAUTION: Concentrated cyanide eluant. Fume cupboard, personal HCN monitor on, not alone. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Copper Elution Test - Column Run - Cyanide-bearing eluate - Pinch point at the hose |  | - Fill the column with 150 mL of preconditioned resin with no voids between resin. - Fill the column with distilled water, calibrate the pump (Step 10), then drain the remaining water from the column. - Run the eluant with the dosing pump at 1 BV/h (150 mL/h, 2.5 mL/min) for 3 hours. Target final elution volume 450 mL; the 150 mL left in the beaker goes to the cyanide-bearing waste. - Direct the eluate to a beaker. Use 2 measuring cylinders alternately to move the eluate to the sample bottles. - Sample the eluate at 30, 60, 90, 120, 150 and 180 minutes, about 75 mL per 30 minutes, into labelled bottles. - Titrate every sample for cyanide as SWI-PRO-MET-205-001 - AgNO3 0.1 M for the concentrated eluate, 0.01 M for dilute solutions. Send the samples for Cu and Fe assay and record the results on the copper elution worksheet. |  |  |  |  |  |  |  |  |  |  |  |  |
| - NaCl Dissolution Test - Salt dust - Precipitate not recorded |  | - Dissolve the NaCl of each vendor and the plant NaCl into 500 mL of solution: 1 M = 30.15 g and 3 M = 90.46 g per 500 mL (97 per cent purity, 58.5 g/mol). - Run a jar test for 50 minutes. - Observe and photograph any precipitate. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Eluant Scale Dissolution with Sulfamic Acid - HCN when acid contacts cyanide-bearing scale - Sulfamic acid contact - Test left unattended |  | - Make the sulfamic acid solutions: 7.5 g sulfamic acid in 300 mL process water (test 1) and in 300 mL raw water (test 2). Mix with the magnetic stirrer. - Weigh 5 g of scale sample. Put it into the sulfamic acid solution inside the fume cupboard, WITHOUT stirring. - Observe and photograph at minute 0, 5, 10, 30, 60, 120 and 240 while any deposit remains. Stay with the test for the full 240 minutes with the personal HCN monitor on. - If HCN above 5 ppm is detected, stop: dilute the solution with water and evacuate. - Send the solution and residue to the cyanide-bearing stream until the scale is shown to be cyanide-free. CAUTION: Acid on cyanide-bearing scale releases HCN. Fume cupboard only, attended for the full test, stop at 5 ppm. |  |  |  |  |  |  |  |  |  |  |  |  |
| - NaCN-NaCl Mixing Test - Toxic mixed solution splash - HCN below pH 10.5 |  | - Work in the fume cupboard with clean, dry equipment. - Measure 85 mL of plant NaCl solution into a 150 mL beaker. Raise its pH to 10.5 or above with caustic before any NaCN is added. - Add 15 mL of plant NaCN solution slowly to the NaCl solution, stirring gently at low speed. Always add the NaCN to the NaCl, never the reverse, to avoid splashing toxic solution. - Check the total is about 100 mL (target 1.0 M NaCN and 0.9 M NaCl), homogenise for about 1 minute, and observe for any precipitate or colour change. - Store in a tightly closed container labelled 'NaCN-NaCl Mix, Toxic'. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Copper Loading Test - Zn(CN)4 Eluant - Bulk hi-cyanide eluant (351 g KCN) - HCN below pH 10.5 - Resin sampling at the loaded resin screen |  | - Take the loaded resin sample at the loaded resin screen in a plastic bag as it discharges, as SWI-PRO-MET-201-012. - Weigh 322.8 g zinc sulphate heptahydrate and 351 g KCN. - Add solid caustic slowly to 800 mL distilled water until the pH is 10.5 or above. The Martabe pH 10 is not used. - Add the KCN slowly and mix until clear. Monitor the pH at every step and hold it at 10.5 to 11 with NaOH. - Dissolve the zinc sulphate in 1000 mL distilled water in a separate container and wait about 30 minutes until clear. - Combine the two solutions watching the pH at all times - stop if it falls below 10.5 (see Open items for the order). Make up to 2.2 L with distilled water and mix until clear. CAUTION: 351 g KCN. Fume cupboard, HCN monitor on, no acid in the work area, not alone and not unattended. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Copper Loading Test - Column Elution - Pinch point at the quick-connect - Hi-cyanide eluate |  | - Wash the loaded resin on a sieve with water. Fill the 150 mL column with 150 mL of resin with no voids. - Connect the pump to the bottom inlet with the quick-connect hose; the eluate leaves at the top through a hose into a beaker. Keep hands clear of the pinch point. - Inject distilled water to remove voids, calibrate the dosing pump (Step 10) and drain the remaining water. - Run the Zn(CN)4 eluant at 2 BV/h (300 mL/h) for 6 hours with no water or air in the hose. - Collect the eluate every hour, hour 0 to 6, into bottles labelled 'hi cyanide' and send for Cu, Fe and Zn assay. - Drain the column into a sample bottle and record the volume. Rinse the resin in 300 mL water for 15 minutes. Send both for Cu, Fe and Zn. - Send the waste liquid to the cyanide-bearing stream (see Open items) and return the resin to the loaded resin at the ReCYN plant. Record the copper loading calculation and assays. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Dosing Pump Calibration - Grundfos DDA - Pump calibrated on water only - Air in the hose |  | - Prepare the dosing pump, measuring cylinder, hoses and fittings, and water. Check they are in good condition. - Press the 100% button. Make sure there are no air gaps in the hose. - Press '>' for the setup screen, turn the dial to 'calibration', press the dial, then click start. - Collect the water the pump draws in the measuring cylinder (see Open items for the hose connections). - Compare the cylinder volume with the panel volume. If they differ, set the panel volume to the measured value, click start, then OK. Repeat from the start if still different. - Check the delivered flow at the test rate - 150 mL/h for Step 4, 300 mL/h for Step 9. Record the calibration in the pump calibration logsheet. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Cyanide-bearing residue to the general drain - Glassware left dirty - Result not traceable to the instrument |  | - Wash down the bench and the fume cupboard working surface. - Clean glassware and return it to the drying rack. - Dispose of residues to the correct waste stream - cyanide-bearing effluent does NOT go to the general drain. - Record the result, the method used and the instrument or balance identity. - Record every value determined on the field or bench data sheet - date, time, shift and operator. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| JSEA-PRO-MET-205-013 | JSEA — Resin Elution Efficiency and Barren Resin Loading Test |
| KBK SOP-PROC-CNREC-02 and CNREC-05 | Cyanide elution and metal elution - operating elution conditions (received 11 Aug 2026) |
| Goldquip resin elution data | Not held |
| Martabe WI (11/01/2025) | Testing NaCl from New Vendor - source of Steps 3 to 5 |
| Martabe WI V2 (07/02/2025) | Preconditioning Resin with Cu Variance - source of Step 2 |
| Martabe WI (07/10/2025) | Testwork Pelarutan Scaling Eluant Garam Menggunakan Sulfamic Acid - source of Step 6 |
| Martabe WI (undated) | IPHK Mixing Larutan Campuran NaCN-NaCl - source of Step 7 |
| DOC-3-MET-MEL-WIN-00113-IE v1.0 | Martabe WI Copper Loading Test (25/01/2025) - source of Steps 8 and 9 |
| DOC-3-MET-PMC-WIN-00120-IE v1.0 | Martabe WI Dosing Pump Grundfos DDA Calibration (25/12/2024) - source of Step 10 |
| Martabe WI (undated) | Copper Adsorption - second source for Steps 3 and 4 |
| DOC-2-MET-MEL-SOP-00087-IE and DOC-IV-MET-CHH-SOP-00039 | Martabe SOPs referenced by the Martabe WIs - not received |
| SWI-PRO-MET-205-001 | Free Cyanide Titration - Silver Nitrate Method |
| SWI-PRO-MET-201-012 | Loaded and Barren Resin Sampling at Screens and Hoppers |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 3. Skin or Eye Contact with Reagent Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 4. HCl Gas or Acid Contact Leave the area upwind. Flush skin or eyes with copious water at the safety shower or eyewash for a minimum of 15 minutes. If breathing is affected call CH19 “EMERGENCY” and call 000. 5. Cuts from Broken Glassware Apply pressure to stop the bleeding, get a trained first aider, and report to the Shift Supervisor. Call CH19 “EMERGENCY” and 000 for a serious cut.