Mt. Morgan SITE WORK INSTRUCTION

Lime Addition and Lime Demand Test

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-205-006 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-205-006 |
| Area | 205 Met Lab - Chemical and Leach Testwork |
| Parent procedure | HM-PRC-VXX-PRO209 Metallurgical Laboratory Chemical and Leach Testwork |
| Classification | Operating |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

DRAFT FOR REVIEW. Martabe work instruction 'Dosing NaOH vs Ca(OH)2 untuk mencapai pH 6,7,8 & 9' added as Section 6 Part B. Not for use until reviewed and approved. JSEA JSEA-PRO-MET-205-006 must be updated for the added hazard row.

# 1  TASK AND SCOPE

Determine how much lime the ore actually needs to hold the target pH through the leach.

Lime demand varies with ore. Dosing to a fixed rate rather than to demand either wastes lime or loses pH control, and losing pH control in a cyanide circuit releases HCN.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| Met lab bench | Physical testwork bench and instrument |

Frequency: On each new ore type and whenever plant lime consumption moves.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO209 - Metallurgical Laboratory Chemical and Leach Testwork. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-205-006 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-205-006.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-205-006 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Contact with sodium hydroxide solution - burn to skin or eyes | Full chemical PPE including face shield and chemical-resistant gloves. Sample drawn slowly from the designated valve. Safety shower and eyewash within reach and proven flowing. |
| Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt | Sampling of solid cyanide done only with the full cyanide PPE set including a gas mask with an A2B2E2K2P3 cartridge. Dust suppression and local extraction confirmed running. No dry sweeping. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Cuts from broken glassware, and burns from hot glassware | Glassware inspected for chips and cracks before use and discarded if damaged. Hot glassware handled with tongs or heat-resistant gloves and set down on a heat mat. Broken glass to the sharps bin, never to the general waste or by hand. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| [JSEA to confirm] Lowering or holding sample pH below 10.5 on a sample that contains cyanide - HCN release | Part B is run only on samples confirmed cyanide-free before the test starts. Any cyanide present: stop, do not add reagent, report to the Shift Supervisor. Part A and all cyanide work keep the pH above 10.5 rule. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-205-006 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Acid-resistant gloves, apron and face shield

- Chemical splash goggles

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Confirm the fume cupboard airflow, the scrubber and its dosing are running before any acid or cyanide work at the bench.

- Confirm the safety shower and eyewash are within reach and proven flowing.

- Confirm the instrument or balance is within its calibration or verification interval.

- Confirm the reagents to be used are in date and correctly labelled.

- Inspect all glassware for chips and cracks and discard anything damaged.

Equipment required:

- Bottles or beakers with stirrers

- pH meter, calibrated

- Lime slurry at known strength

- Pipettes

- Balance

- Stopwatch

- [M] Jar test stirrer, beakers (glass) for 500 mL samples

- [M] Hydrated lime (Ca(OH)2) and caustic (NaOH), weighed doses

- [M] Camera for settling record

- [M] Filter apparatus and sample bottles for assay splits

# 6  STEPS

Part A - Lime demand to the leach target pH

1.  Prepare the ore slurry at the plant leach density.

2.  Measure and record the natural pH before any addition.

3.  Add lime slurry in measured increments, stirring and allowing the pH to stabilise between additions.

4.  Record pH against cumulative lime added.

5.  Continue past the target pH so the curve shape either side is known.

6.  Hold the slurry at the target pH and record any further lime needed over the leach residence time - that is the demand the plant actually has to meet.

7.  Report the lime addition to reach target and the maintenance demand separately.

Part B - Neutralisation reagent comparison: NaOH versus Ca(OH)2 to pH 6, 7, 8 and 9 [M]

[M] = taken from the Martabe team work instruction "Dosing NaOH vs Ca(OH)2 untuk mencapai pH 6,7,8,&9" (undated). [CONFIRM] = unspecified or inconsistent in the source; resolve before this instruction is approved for use. Part A (original steps) is unchanged.

Purpose [M]: find the NaOH and the Ca(OH)2 consumption needed to bring the sample to pH 6, 7, 8 and 9, and compare the two reagents. Two runs on 500 mL of sample SP09: Run 1 with hydrated lime, Run 2 with caustic.

STOP condition (added at review, not in the source): this test brings a sample to pH values BELOW 10.5. Run it only on a sample confirmed free of cyanide. If cyanide is present at any level, do not start - HCN will be released.

Run 1 - hydrated lime [M]

1.  Take 500 mL of sample SP09 in a glass beaker. [CONFIRM] SP09 is not defined in the source - state what the sample is and its origin.

2.  Stir the sample with the jar test stirrer until homogeneous.

3.  Measure and record the sample pH before any lime is added.

4.  Take 100 mL of the feed, code A1-0, for base metal assay.

5.  Add lime slowly until the pH reaches 6. Record the mass of lime added.

6.  Wait 5 minutes so the lime reaction goes to completion.

7.  Repeat the slow addition and the 5 minute wait for pH 7, 8 and 9 in turn, recording the lime mass added at each pH. [CONFIRM] the source says 'repeat steps 4 and 5'; this is read as the addition and wait steps above, not the A1-0 sampling.

8.  After the 5 minute wait at pH 9, let the solids settle to the bottom of the beaker.

9.  Photograph the sample to record its visual condition.

10.  Record the time taken for the particles to settle to the bottom of the beaker.

11.  Photograph the sample while settling and the settled particles (observe for a maximum of 2 hours).

12.  When settled, filter the sample. Submit 100 mL of solution coded A1-1 and 50 g of the solids coded A1-2 for base metal assay.

Run 2 - caustic [M]

13.  Repeat Run 1 steps 1 to 12 on a fresh 500 mL of sample SP09, adding caustic (NaOH) in place of lime. Record the mass of caustic added at each pH. Sample codes: B1-0 (feed, 100 mL), B1-1 (solution, 100 mL), B1-2 (solids, 50 g). [CONFIRM] the source Run 2 text still says 'add lime' at the first addition step; caustic is read as intended.

Assay and records [M]: request the full dissolved base-metal assay on every coded sample - Al, Cd, Cu, Fe, Mn, Ni, Zn, Cr, Pb, Na, Hg, As, TSS, TDS, Mg, Ca, SO4 and Cl. Record lime mass and caustic mass at each pH, settling time, photographs and the sample codes A1-0/1/2 and B1-0/1/2. Compare the consumption of the two reagents at each pH.

# 7  ON COMPLETION

- Wash down the bench and the fume cupboard working surface.

- Clean glassware and return it to the drying rack.

- Dispose of residues to the correct waste stream - cyanide-bearing effluent does NOT go to the general drain.

- Record the result, the method used and the instrument or balance identity.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- KBK-MIR-MP-PRO-OPE-SOP-0002 Uji Penambahan Kapur

- Martabe work instruction 'Dosing NaOH vs Ca(OH)2 untuk mencapai pH 6,7,8,&9' (Indonesian, undated) - Part B source