Safe Work Instruction

Leach Tank Sampling Round - 031-TK-001 Launder and Discharge

This document is the property of Heritage Minerals with all rights are reserved in respect of it. This document cannot be reproduced without the written consent of Heritage Minerals

# Purpose and Scope

This Safe Work Instruction is required so that the mechanical and operational integrity of the system is kept intact. It assists operators and mechanical technicians alike to identify possible problems before they happen.  It will help ensure that when personnel are performing this task it is performed in a safe and secure manner, to ensure the operational integrity of the machine and applies when this task is performed either by itself or in conjunction with other tasks in the area.

A JSA or Take 5 must be completed and discussed with the Supervisor if any variation to this SWI is necessary.

# RESPONSIBILITIES AND AUTHORITY

| What | Who | When |
| --- | --- | --- |
| Conform to procedure: Implement Changes: Change procedure: Review: Authorisation: | All personnel Anyone Training Facilitator Working party of content experts Manager | At all times As required As required On change & yearly On change |

# PPE REQUIREMENTS

- Safety helmet and safety glasses

- Chemical splash goggles and face shield

- High-visibility long-sleeved shirt and long trousers

- Safety boots with sound tread - nitrile PVC boots at the sample point

- Chemical resistant suit, nitrile rubber gloves and apron

- Personal HCN gas monitor, calibrated and in test date

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

In the event of an emergency

Call on CH19 “EMERGENCY, EMERGENCY, EMERGENCY” on the project to make everyone aware, call 000 for emergency services, police, fire or ambulance, you will need to stay calm and state when requested by a responder:

• Your Name. • Your Location. • Type of Emergency; and • Assistance Required.

| Part 1: Information |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Title: |  |  | SWI-PRO-MET-201-003 - Leach Tank Sampling Round - 031-TK-001 Launder and Discharge |  |  |  |  |  |  |  |  |  |  |  |
| Issued Date: |  |  | 11/08/2026 |  |  |  |  | Next Review Date: |  |  |  | 11/08/2027 |  |  |
| Document Owner: |  |  | Processing |  |  |  |  | JSEA ID: |  |  |  | JSEA-PRO-MET-201-003 |  |  |
| Part 2: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Description of work: |  |  |  |  |  | Set leach feed pH, dissolved oxygen, free and WAD cyanide, solids percentage and solution and solid assay. Dissolved oxygen in the leach feed is a critical process parameter - low DO points to insufficient oxygen supplementation and directly reduces gold dissolution. Area: 031 Leaching. Points and equipment covered: 031-TK-001 - Leach tank, launder and discharge 031-PP-166 - Leach feed sampling pump 031-SC-002 - Screen in the leach circuit Frequency: Hourly spot sample, composited to four 12-litre composites per shift. This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO205 - Plant Sampling and Metallurgical Data Collection. Read that procedure before carrying out this task for the first time. Register line: SWI-PRO-MET-201-003 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-201-003. This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress. |  |  |  |  |  |  |  |  |
| Potential Hazards: |  |  |  |  |  | Hydrogen cyanide gas released at the open sample point — Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. Splash of cyanide-bearing slurry or solution to skin or eyes — Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. Fall from a tank top, launder platform, column platform or access ladder — Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. Contact with an agitator, sample cutter, pump or screen that starts without warning — Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. Slip, trip or fall on wet or slurry-covered walkways around sample points — Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. Manual handling injury from carrying sample buckets, containers and composite drums — Sample volume kept to the schedule - no over-filling. Two-person lift or a trolley for composite containers above the site manual handling limit. Route cleared before lifting. Working alone in a cyanide area where a collapse would not be seen — Cyanide-area sampling is not done alone. Control room notified at the start and end of every round. Radio check-in at the interval set by the Shift Supervisor. Non-representative sample leading to a wrong process decision — Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. Cross-contamination from a container or cutter not cleaned between points — Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. Confined space atmosphere at a tank top hatch, launder or hopper opening — No entry. Sampling is done from outside the opening only. Confined space entry, if it is ever needed for a sample point, requires a permit, atmosphere testing, isolation, a standby person and a rescue plan under the site confined space procedure. The full step-by-step hazard analysis, with the risk ranking, is in JSEA-PRO-MET-201-003 Section 4. |  |  |  |  |  |  |  |  |
| PERSONAL PROTECTIVE EQUIPMENT (PPE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Part 3: Safe Work Instruction Steps |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Job Number (Hazards/Cautions) |  | Application Method |  |  |  |  |  |  | Visual Reference |  |  |  |  |  |
| - Pre-start Check - Working alone in a cyanide area - Gas monitor or fixed detection not healthy - Safety shower or eyewash not proven flowing - Pump line flow not normal |  | - Confirm you are trained and signed off against this SWI, signed on to JSEA-PRO-MET-201-003 at a communication session, and authorised by the Shift Supervisor. - Confirm a second person is in the area. Cyanide-area sampling is not done alone. - Verify flow on the leach tank sampling pump line is normal - no surging and no blockage. - Confirm the plant is in steady-state operation - normal operation for a minimum of 15 to 20 minutes before sampling. A sample taken during a swing is not representative. - Notify the control room or DCS operator that the sampling round is starting, and which points it covers. - Confirm the personal gas monitor is on, in calibration date and reading clean, and that fixed detection in the area is healthy. - Confirm the safety shower and eyewash nearest the point are within reach and proven flowing. - Label every container BEFORE sampling - point, date, time and shift. - Rinse the container, cutter or sieve with process water and then with the stream being sampled. Discard the rinse. Equipment Required : - Sampling bucket 5 to 8 L - Marcy scale - pH meter - DO meter - Free cyanide titration kit - standardised AgNO3 - Rhodanine indicator - Burette 50 mL - Pipette 10 or 25 mL - Conical flask 250 mL - Burette stand and clamp - Wash bottle - Bottles 250 and 500 mL - Filter press and filter paper - Spatula - Distilled water - Personal protective equipment as listed in PPE Requirements |  |  |  |  |  |  |  |  |  |  |  |  |
| - Sample Collection - HCN released at the open sample point - Fall from the tank top or access ladder - Confined space atmosphere at the tank top hatch or launder - Equipment starting without warning |  | - Start the leach feed sampling pump 031-PP-166. - Allow the first 5 to 10 seconds of flow to discharge to drain as a line flush. - Collect a minimum of 4 litres of slurry into the sampling bucket. - Stop the leach feed sampling pump 031-PP-166. - Stir the sample thoroughly with the spatula to homogenise it before splitting into two containers. CAUTION: Sample from outside the opening only. Do not enter a tank top hatch, launder or hopper opening. Carry sample containers in a bag or hoist them, not in the hand on a ladder. |  |  |  |  |  |  |  |  |  |  |  |  |
| - pH and Dissolved Oxygen - Dissolved oxygen reading changed by air exposure - Meter out of calibration - wrong pH |  | - Determine pH. Calibrate once per shift against pH 4, 7 and 10 buffers, rinse and dry the electrode, and immerse fully. - Wait about 30 seconds for a stable reading. Record the value and temperature. - Determine dissolved oxygen IMMEDIATELY after collection to prevent atmospheric exchange. - Rinse the DO probe. Do not wipe the membrane hard. Immerse the probe and keep a gentle flow across the membrane. - Wait 30 to 60 seconds. Record the value and temperature. CAUTION: Delay between collection and the DO reading lets atmospheric oxygen change the result. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Filtration and Free Cyanide Sample - Cyanide volatilising from the filtrate - Splash of cyanide-bearing filtrate - Bottles mislabelled |  | - Filter about 2000 mL through the filter press to obtain a clear filtrate. - Collect the filtrate into three labelled bottles - CN Free manual, CN Free Lab, WAD CN Lab. - Titrate the CN Free manual filtrate straight after filtration to minimise cyanide volatilisation. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Per Cent Solids and Assay Samples - Scale not zeroed - wrong per cent solids - Assay sample not submitted with the cake |  | - Determine per cent solids on the Marcy scale. - Filter 1 litre for solution and solid assay. - Dry the cake and submit both the solution and the cake to the laboratory. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Free Cyanide Titration - Silver Nitrate Method - Splash of silver nitrate or cyanide filtrate - Endpoint overshot - wrong free cyanide result |  | - Rinse the burette with distilled water, then condition it three times with standardised AgNO3. - Fill the burette with standardised AgNO3 and remove air bubbles from the tip. - Pipette 10 mL of the filtrate into a 250 mL conical flask. - Add 3 to 5 drops of rhodanine indicator. The solution turns pale yellow. - Add AgNO3 dropwise while swirling continuously. - As the endpoint approaches a salmon pink precipitate forms and redissolves slowly on swirling - slow the addition at this point. - Continue dropwise until a permanent salmon pink colour holds for at least 30 seconds without swirling. That is the endpoint. - Record the final burette reading and calculate the free cyanide concentration. |  |  |  |  |  |  |  |  |  |  |  |  |
| - Completion and Clean Up - Sample valve left weeping - Samples not handed over with a signed record - Control room not told the round is complete |  | - Close the sample valve or stop the sample pump and confirm the point is not weeping. - Wash down the point and the surrounding walkway. Leave nothing on the grating. - Record sampling time, operator name and the operating conditions read at the time - flow, density and any instrument value available. - Deliver the labelled samples to the laboratory or to the composite station as the schedule requires, and sign the handover. - Notify the control room that the round is complete. - Record the result, the method used and the instrument or balance identity on the field or bench data sheet - date, time, shift, operator and every value determined. Make the register or logbook entry and any handover signature. - Record any step not completed, with the reason. - Report to the Shift Supervisor, and record, any control in Part 2 found not in place. |  |  |  |  |  |  |  |  |  |  |  |  |

| Referenced Documents |  |
| --- | --- |
| Document ID | Document Title |
| HM-PRC-VXX-PRO205 | Plant Sampling and Metallurgical Data Collection |
| JSEA-PRO-MET-201-003 | JSEA — Leach Tank Sampling Round - 031-TK-001 Launder and Discharge |
| HM-MMM-WHS-REG-XXX-R00-SWI-SWMS | SWI / SWMS Register — tab SWI-MET |
| HM-PRC-V01-PRO004 | Leach Circuit |
| Mt. Morgan site procedure 4 | Leach Tank Sampling [LIVE] |
| KBK-MIR-MP-PRO-MET-SOP-0048 | Pengambilan Sampel dan Pengukuran Profil Tangki Leaching, received 11 Aug 2026 |
| KBK-MIR-MP-PRO-MET-SOP-0046 | Pengukuran Oksigen Terlarut, received 11 Aug 2026 |
| KBK-MIR-MP-PRO-MET-SOP-0045 | Pengukuran Densitas Lumpur, received 11 Aug 2026 |
| 4034-044-VE-003 Rev B | Glencore Hypersparge supersonic gas sparger instructions, received 11 Aug 2026 |

In the event of an emergency

1. HCN Gas Alarm If the personal monitor or fixed detection alarms (5 ppm alarm, 10 ppm high-high), stop work, leave the area upwind and call CH19 “EMERGENCY”. Do not re-enter until the Shift Supervisor clears the area. 2. Contact with Moving Equipment If a person is caught by or struck by an agitator, pump or screen, hit the nearest emergency stop, call CH19 “EMERGENCY” and call 000. Do not approach the equipment until it is isolated and locked out. 3. Suspected Cyanide Exposure If a person becomes dizzy, short of breath or collapses, call CH19 “EMERGENCY”, call 000, and bring the cyanide antidote kit and a trained first aider. Do not give mouth-to-mouth resuscitation. 4. Skin or Eye Contact with Slurry or Filtrate Flush with copious water at the safety shower or eyewash for a minimum of 15 minutes. Remove contaminated clothing while flushing. Report to the first aider. 5. Person Down at a Tank Top, Launder or Hopper Opening Do not enter the opening. Call CH19 “EMERGENCY” and call 000. Rescue is by the trained rescue team under the site confined space procedure only. 6. Fall from Height Do not move the injured person unless they are in danger. Call CH19 “EMERGENCY”, call 000, and notify the Shift Supervisor.