Mt. Morgan SITE WORK INSTRUCTION

CIL Tail Sampling at Carbon Safety Screen 032-SC-003 Undersize

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-201-008 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-201-008 |
| Area | 032 Carbon in Leach |
| Parent procedure | HM-PRC-VXX-PRO205 Plant Sampling and Metallurgical Data Collection |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

SAFETY-CRITICAL FINDING - READ BEFORE STARTING. 032-SC-003 is the SOLE carbon barrier between the CIL circuit and the resin circuit. The Control Philosophy mark-up dated 07-08-2026 deletes every automatic action that closed feed valves 032-XV-003 and 032-XV-004 - item PCP-054 removes the high-level close, PCP-079 removes ILHH-041001 closing them, and PCP-122 removes the same action again from Section 3.1.7. RA-02 Rev A had already found that 032-XV-004 had no interlock. After the mark-up NEITHER valve has one. The barrier is this screen and the operator watching it. Carbon seen in the undersize is reported immediately.

# 1  TASK AND SCOPE

Set the CIL tail grade - the number that closes the gold balance across the leach and adsorption circuits.

Check that carbon is not reporting to the undersize. 032-SC-003 is the sole carbon barrier between the CIL circuit and the resin circuit.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 032-SC-003 | Carbon safety screen - undersize |
| 032-XV-003 / 032-XV-004 | Feed valves - position confirmed manually before sampling |
| 032-XM-012 | CIL tails automatic sampler - the manual sample cross-checks it |

Frequency: Hourly spot sample, composited per shift. Carbon check on every sample.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO205 - Plant Sampling and Metallurgical Data Collection. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-201-008 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-201-008.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-201-008 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Slip, trip or fall on wet or slurry-covered walkways around sample points | Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. |
| Manual handling injury from carrying sample buckets, containers and composite drums | Sample volume kept to the schedule - no over-filling. Two-person lift or a trolley for composite containers above the site manual handling limit. Route cleared before lifting. |
| Working alone in a cyanide area where a collapse would not be seen | Cyanide-area sampling is not done alone. Control room notified at the start and end of every round. Radio check-in at the interval set by the Shift Supervisor. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-201-008 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Confirm the plant is in steady-state operation - normal operation for a minimum of 15 to 20 minutes before sampling. A sample taken during a swing is not representative.

- Notify the control room or DCS operator that the sampling round is starting, and which points it covers.

- Confirm the personal gas monitor is on, in calibration date and reading clean, and that fixed detection in the area is healthy.

- Confirm the safety shower and eyewash nearest the point are within reach and proven flowing.

- Label every container BEFORE sampling - point, date, time and shift.

- Rinse the container, cutter or sieve with process water and then with the stream being sampled. Discard the rinse.

Equipment required:

- Sampling bucket 5 to 8 L

- 1 mm sieve

- Marcy scale

- Filter press and filter paper

- Bottles 250 mL

- Spatula

- Personal protective equipment as Section 5

# 6  STEPS

1.  Confirm valve positions on 032-XV-003 and 032-XV-004 by eye before approaching. There is no automatic protection - see the finding below.

2.  Flush the point and discard the first flow.

3.  Collect 4 litres of undersize slurry.

4.  Pass a measured volume over the 1 mm sieve and inspect the retained solids for carbon. ANY carbon in the undersize is reported to the Shift Supervisor immediately, before the round continues.

5.  Determine per cent solids on the Marcy scale.

6.  Filter and bottle for tail assay and for WAD cyanide.

7.  Record the result against the reading from automatic sampler 032-XM-012 taken at the same time.

# 7  ON COMPLETION

- Close the sample valve or stop the sample pump and confirm the point is not weeping.

- Wash down the point and the surrounding walkway. Leave nothing on the grating.

- Record sampling time, operator name and the operating conditions read at the time - flow, density and any instrument value available.

- Deliver the labelled samples to the laboratory or to the composite station as the schedule requires, and sign the handover.

- Notify the control room that the round is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- 4034-PR-PRO-002 Sampling Protocol item 5 - the sample point is still marked (TBC) in the protocol

- 4034-004-VE-025 Rev B Goldquip vibrating screen IOM (032-SC-003), received 11 Aug 2026

- RA-02 Carbon Contamination Register Rev A

- HM-PRC-V01-PRO005 Carbon in Leach (CIL) Circuit