Mt. Morgan SITE WORK INSTRUCTION

Loaded and Barren Resin Sampling at Screens and Hoppers

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-201-012 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-201-012 |
| Area | 041 / 051 / 071 / 081 Resin circuits |
| Parent procedure | HM-PRC-VXX-PRO205 Plant Sampling and Metallurgical Data Collection |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  TASK AND SCOPE

Set the metal loading on resin leaving adsorption and the residual loading on resin returning from elution.

The loaded-to-barren pair is the direct measure of elution efficiency on the resin circuit.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 041-SC-004 / 041-SC-016 | Metal adsorption resin recovery and safety screens |
| 051-SC-005 / 051-SC-006 / 051-SC-020 | Cyanide adsorption resin screens |
| 041-HP-017 | Metal loaded resin hopper |

Frequency: Every resin transfer, both directions.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO205 - Plant Sampling and Metallurgical Data Collection. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-201-012 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-201-012.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-201-012 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Slip, trip or fall on wet or slurry-covered walkways around sample points | Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. |
| Manual handling injury from carrying sample buckets, containers and composite drums | Sample volume kept to the schedule - no over-filling. Two-person lift or a trolley for composite containers above the site manual handling limit. Route cleared before lifting. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-201-012 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Confirm the plant is in steady-state operation - normal operation for a minimum of 15 to 20 minutes before sampling. A sample taken during a swing is not representative.

- Notify the control room or DCS operator that the sampling round is starting, and which points it covers.

- Confirm the personal gas monitor is on, in calibration date and reading clean, and that fixed detection in the area is healthy.

- Confirm the safety shower and eyewash nearest the point are within reach and proven flowing.

- Label every container BEFORE sampling - point, date, time and shift.

- Rinse the container, cutter or sieve with process water and then with the stream being sampled. Discard the rinse.

Equipment required:

- Sample scoop or cutter

- 0.9 mm sieve

- Sample bottles, labelled

- Process water hose

- Personal protective equipment as Section 5

# 6  STEPS

1.  Confirm with the control room that a resin transfer is in progress and which direction it is running.

2.  Sample the screen oversize as the resin discharges, taking increments across the whole transfer rather than one grab.

3.  Wash the resin free of slurry over the 0.9 mm sieve.

4.  Bottle, label with the transfer number and direction, and submit to the laboratory.

5.  Record transfer number, direction, volume and time against the sample.

# 7  ON COMPLETION

- Close the sample valve or stop the sample pump and confirm the point is not weeping.

- Wash down the point and the surrounding walkway. Leave nothing on the grating.

- Record sampling time, operator name and the operating conditions read at the time - flow, density and any instrument value available.

- Deliver the labelled samples to the laboratory or to the composite station as the schedule requires, and sign the handover.

- Notify the control room that the round is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- Mt. Morgan site procedure 9. Metal Elution Sampling [LIVE] - covers part of this task

- KBK SOP-PROC-CNREC-01, -04, -06 and -07 resin transfer procedures, received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0049 and SOP-0058, received 11 Aug 2026

- 4034-004-VE-025 Rev B Goldquip vibrating screen IOM, received 11 Aug 2026