Mt. Morgan SITE WORK INSTRUCTION

Screen and Cyclone Performance Survey - Size Split Determination

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-203-003 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-203-003 |
| Area | 203 Plant Surveys |
| Parent procedure | HM-PRC-VXX-PRO207 Plant Surveys and Circuit Performance Assessment |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  TASK AND SCOPE

Determine the actual size split across each screen and cyclone against what the design assumes.

A screen or cyclone not doing what the flowsheet says it does moves the problem downstream, usually into the mill or the adsorption circuit.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 021-SC-001 | Trash screen |
| 032-SC-002/003 | Loaded carbon and carbon safety screens |
| 041 / 051 | Adsorption interstage and recovery screens |
| Cyclones | Overflow and underflow |

Frequency: Quarterly, and after any panel change or aperture change.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO207 - Plant Surveys and Circuit Performance Assessment. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-203-003 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-203-003.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-203-003 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Hearing damage in the mill, screen, compressor and blower areas | Hearing protection mandatory in signed areas. Double protection at the mill and compressor. Time at the point kept to what the task needs. |
| Inhalation of or contact with solid reagent - cyanide briquettes, lime or salt | Sampling of solid cyanide done only with the full cyanide PPE set including a gas mask with an A2B2E2K2P3 cartridge. Dust suppression and local extraction confirmed running. No dry sweeping. |
| Slip, trip or fall on wet or slurry-covered walkways around sample points | Spillage cleaned up immediately and the point left clean. Walkways kept clear of hoses, buckets and containers. Safety boots with sound tread. Report any damaged or missing grating before use. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-203-003 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Hearing protection

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Notify the control room that the task is starting, and where you will be.

- Confirm the personal gas monitor is on, in calibration date and reading clean.

- Confirm the safety shower and eyewash nearest the work are within reach and proven flowing.

- Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress.

Equipment required:

- Sieve set and Ro-Tap shaker

- Filter press and filter paper

- Drying oven

- Balance

- Sample containers by stream

- Field data sheets

# 6  STEPS

1.  Sample feed, oversize and undersize on the screen, or feed, overflow and underflow on the cyclone, at the same time.

2.  Take increments across the full width or the full discharge, not one grab from the near end.

3.  Filter, dry and weigh each stream.

4.  Screen each to the full sieve set and record the mass retained on each aperture.

5.  Calculate the partition curve and the actual cut size.

6.  Compare the cut size against the stated aperture for the screen, and against the design cut for the cyclone.

7.  Report any screen where the cut size and the aperture do not agree - it usually means a torn or wrong panel.

# 7  ON COMPLETION

- Leave the area clean. Recover spillage to the drain, not to the ground.

- Return all equipment to its storage point.

- Record what was done, what was found and anything not completed.

- Notify the control room that the task is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- KBK-MIR-MP-PRO-OPE-SOP-0008 Cyclone Efficiency

- KBK-MIR-MP-PRO-MET-SOP-0029 Sizing Harian COF and SOP-0020 Distribusi Logam dan Ukuran, both received 11 Aug 2026

- MM-4034-033 Screen Aperture Register

- 4034-004-VE-025 and 4034-011-VE-022 Goldquip screen manuals, received 11 Aug 2026