Mt. Morgan SITE WORK INSTRUCTION

Residence Time and Tracer Test on Leach and Adsorption Trains

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-203-004 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-203-004 |
| Area | 203 Plant Surveys |
| Parent procedure | HM-PRC-VXX-PRO207 Plant Surveys and Circuit Performance Assessment |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  TASK AND SCOPE

Measure the actual residence time and the degree of short-circuiting in the leach and adsorption trains.

Design residence time assumes ideal mixing. Real tanks short-circuit, and a train that short-circuits loses recovery no matter how good the chemistry is.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 031-TK-001 | Leach tank |
| 032-TK-002 to -006 | CIL train |
| 041-TK-007/008 | Metal adsorption |
| 051-TK-009/010 | Cyanide adsorption |

Frequency: Once at commissioning, then after any change to feed rate, agitator or tank configuration.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO207 - Plant Surveys and Circuit Performance Assessment. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-203-004 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-203-004.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-203-004 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Working alone in a cyanide area where a collapse would not be seen | Cyanide-area sampling is not done alone. Control room notified at the start and end of every round. Radio check-in at the interval set by the Shift Supervisor. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-203-004 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Notify the control room that the task is starting, and where you will be.

- Confirm the personal gas monitor is on, in calibration date and reading clean.

- Confirm the safety shower and eyewash nearest the work are within reach and proven flowing.

- Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress.

Equipment required:

- Tracer approved for use in a cyanide circuit

- Sample containers, timed series, pre-labelled

- Stopwatch

- Field data sheets

# 6  STEPS

1.  Agree the tracer with the Metallurgist and confirm it is compatible with a cyanide circuit and with the downstream product. Do NOT introduce anything to the circuit that has not been approved.

2.  Confirm the circuit is at steady state and will be held there for the full test.

3.  Inject the tracer as a pulse at the train inlet and start the clock at injection.

4.  Sample the outlet at the stated interval for at least three theoretical residence times.

5.  Sample intermediate tanks where the arrangement allows it, so short-circuiting can be located, not just detected.

6.  Analyse the tracer concentration series and construct the residence time distribution.

7.  Compare the measured mean residence time against the design, and report the degree of short-circuiting by tank.

# 7  ON COMPLETION

- Leave the area clean. Recover spillage to the drain, not to the ground.

- Return all equipment to its storage point.

- Record what was done, what was found and anything not completed.

- Notify the control room that the task is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- No direct source held. Written from first principles.

- Plant Operating Manual Sections 3.4 and 3.5 - train configuration and design residence time