Mt. Morgan SITE WORK INSTRUCTION

Oxygen Utilisation and Sparger Performance Survey

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-203-012 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-203-012 |
| Area | 203 Plant Surveys |
| Parent procedure | HM-PRC-VXX-PRO207 Plant Surveys and Circuit Performance Assessment |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  TASK AND SCOPE

Measure how much of the oxygen injected into the leach is actually being used, and whether the spargers are delivering it.

Oxygen is a direct input to gold dissolution. A blocked or worn sparger costs recovery quietly.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 031-TK-001 | Leach tank - oxygen spargers |
| Hypersparge | Supersonic gas spargers DN15 and DN25 |

Frequency: Quarterly, and after any sparger clean or replacement.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO207 - Plant Surveys and Circuit Performance Assessment. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-203-012 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-203-012.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-203-012 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Release from a pressurised sample line, hose or fitting | Confirm the sample line is not blocked before opening. Open slowly and stand clear of the discharge path. Report any weeping fitting rather than tightening it under pressure. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Working alone in a cyanide area where a collapse would not be seen | Cyanide-area sampling is not done alone. Control room notified at the start and end of every round. Radio check-in at the interval set by the Shift Supervisor. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-203-012 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Notify the control room that the task is starting, and where you will be.

- Confirm the personal gas monitor is on, in calibration date and reading clean.

- Confirm the safety shower and eyewash nearest the work are within reach and proven flowing.

- Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress.

Equipment required:

- DO meter, calibrated

- Sample containers

- Stopwatch

- Field data sheets

- Oxygen flow readings from the control system

# 6  STEPS

1.  Record the oxygen supply pressure and flow to each sparger from the control system.

2.  Measure dissolved oxygen at several depths and positions in the tank, not at one point. A single reading at the launder does not describe the tank.

3.  Take the DO reading immediately on sampling - atmospheric exchange starts as soon as the sample is drawn.

4.  Calculate oxygen utilisation from the injected flow and the measured dissolved oxygen against the consumption implied by the leach rate.

5.  Compare the sparger operating pressure against the Hypersparge instructions. A sparger operating below its design pressure is not atomising.

6.  Inspect the sparger condition against the vendor criteria where access allows.

7.  Report utilisation, the DO profile and any sparger due for cleaning or replacement.

# 7  ON COMPLETION

- Leave the area clean. Recover spillage to the drain, not to the ground.

- Return all equipment to its storage point.

- Record what was done, what was found and anything not completed.

- Notify the control room that the task is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- 4034-044-VE-003 Rev B Glencore Hypersparge supersonic gas sparger installation and operating instructions, received 11 Aug 2026

- KBK-MIR-MP-PRO-MET-SOP-0046 Pengukuran Oksigen Terlarut, received 11 Aug 2026

- HM-PRC-V01-PRO004 Leach Circuit and SWI-PRO-OPR-031-004 Oxygen Sparger Inspection and Cleaning