Mt. Morgan SITE WORK INSTRUCTION

Automatic versus Manual Sample Bias Check and Reconciliation

Standard Work Instruction  ·  Heritage Minerals  ·  Mt. Morgan Processing Plant

| Document number | SWI-PRO-MET-207-006 |
| --- | --- |
| JSEA reference | JSEA-PRO-MET-207-006 |
| Area | 207 Automatic Sampling and Online Analysers |
| Parent procedure | HM-PRC-VXX-PRO211 Automatic Sampling and Online Analyser Operation |
| Classification | Safety-critical |
| Revision | Rev A |
| Date | 11 August 2026 |
| Prepared by | GGT (cost code 4034-033) |
| Reviewed by | ________________________ |
| Approved by | ________________________ |

# 1  TASK AND SCOPE

Compare what the automatic samplers report against a manual sample taken at the same point and time.

This is the only check that an automatic sampler is telling the truth, and it is the one that most often gets skipped.

Points and equipment covered:

| Tag / point | Description |
| --- | --- |
| 022-XM-011 / -017 | IsaMill feed |
| 032-XM-012 | CIL tails |
| 041-XM-013 | Metal adsorption tails |
| 051-XM-014 | Final tails |

Frequency: Monthly on every sampler, and after any sampler repair or cutter change.

This instruction sits under Standard Work Procedure HM-PRC-VXX-PRO211 - Automatic Sampling and Online Analyser Operation. Read that procedure before carrying out this task for the first time.

Register line: SWI-PRO-MET-207-006 in HM-MMM-WHS-REG-XXX-R00-SWI-SWMS, tab SWI-MET. The matching hazard analysis is JSEA-PRO-MET-207-006.

# 2  WHO MAY DO THIS

- Trained and signed off against this instruction.

- Signed on to JSEA JSEA-PRO-MET-207-006 at a communication session.

- Site inducted, with current cyanide awareness and gas detection competency where the area requires it.

- Authorised by the Shift Supervisor before the task starts.

This is a safety-critical task. It is not carried out alone in a cyanide area, and not without the Shift Supervisor knowing it is in progress.

# 3  HAZARDS SPECIFIC TO THIS TASK

| Hazard | Control |
| --- | --- |
| Hydrogen cyanide gas released at the open sample point | Personal HCN monitor worn and switched on, in calibration date. Fixed detection confirmed healthy - alarm 5 ppm, high-high 10 ppm. Sample point approached from upwind. pH of the stream confirmed above 10.5 before opening. Second person in sight and clear. Cyanide antidote kit on site and a trained first aider on shift. Withdraw upwind and report on any reading above the site action level. |
| Splash of cyanide-bearing slurry or solution to skin or eyes | Sample valve opened slowly with the container positioned first and the body out of the spray path. Face shield, chemical splash goggles, chemical-resistant gloves and apron. Never open a sample valve whose discharge cannot be seen. Safety shower and eyewash proven flowing before the round starts. |
| Contact with an agitator, sample cutter, pump or screen that starts without warning | Much of the plant is automated and equipment can start or stop without warning. Guards confirmed in place before approaching. Control room notified before the round starts and again on completion. Isolation and lock-out before any guard or cutter housing is opened. |
| Fall from a tank top, launder platform, column platform or access ladder | Fixed platforms, stairways and handrails used in preference to any other access. Harness and fall arrest where no fixed platform exists. Three points of contact on ladders. No sampling at height alone. Sample containers carried in a bag or hoisted, not in the hand on a ladder. |
| Non-representative sample leading to a wrong process decision | Line flushed for the stated time before collecting. Sample taken at the same point, in the same way and at the same frequency every time. Container labelled BEFORE the sample is taken, with point, date, time and shift. Steady-state confirmed for 15 to 20 minutes before sampling. A sample taken off-condition is marked as such or discarded. |
| Cross-contamination from a container or cutter not cleaned between points | Bucket, container, cutter and sieve rinsed with process water and then with the stream being sampled, and the rinse discarded, before every sample. Dedicated containers for high-grade streams. Labels checked against the schedule before handover. |

The full step-by-step hazard analysis, with the risk ranking, is in JSEA JSEA-PRO-MET-207-006 Section 4.

# 4  PPE

- Hard hat

- Safety glasses

- High-visibility long-sleeved shirt and long trousers

- Safety boots

- Gloves appropriate to the task

- Personal HCN gas monitor, calibrated and in test date

- Chemical splash goggles and face shield

- Nitrile rubber gloves

- Nitrile PVC boots

- Chemical resistant suit

- Full or half gas mask with A2B2E2K2P3 cartridge, carried and available for immediate use

- Harness and fall arrest where no fixed platform exists

# 5  BEFORE YOU START

Every item below must be true. If one is not, stop and report it.

- Notify the control room that the task is starting, and where you will be.

- Confirm the personal gas monitor is on, in calibration date and reading clean.

- Confirm the safety shower and eyewash nearest the work are within reach and proven flowing.

- Confirm the area is fit - no restricted access, no gas alarm, no spill response in progress.

Equipment required:

- Manual sampling equipment per the Area 201 instructions

- Pre-labelled containers

- Stopwatch

- Field data sheets

# 6  STEPS

1.  Arrange the check with the control room and the laboratory so both samples are analysed in the same batch.

2.  Take the manual sample at the same point and over the same period the automatic sampler composites over. A grab against a composite is not a comparison.

3.  Take at least ten paired samples across the period - a single pair proves nothing.

4.  Submit the pairs to the laboratory as blind duplicates where possible.

5.  Plot the automatic result against the manual result and test for bias, not just for scatter. A consistent offset in one direction is bias; scatter about the line is precision.

6.  Where bias is found, inspect the cutter and the sampler installation before concluding the laboratory is at fault.

7.  Report the bias with the monthly close and correct the accounting where a bias is confirmed.

8.  Repeat the check after any correction.

# 7  ON COMPLETION

- Leave the area clean. Recover spillage to the drain, not to the ground.

- Return all equipment to its storage point.

- Record what was done, what was found and anything not completed.

- Notify the control room that the task is complete.

# 8  RECORDS

- Field or bench data sheet - date, time, shift, operator, and every value determined.

- Register or logbook entry and any handover signature.

- Any step not completed, recorded with the reason.

- Any control in Section 3 found not in place, reported to the Shift Supervisor and recorded.

# 9  REFERENCE

- 4034-PR-PRO-002 Sampling Protocol - the manual points to compare against

- SWI-PRO-MET-201-001 to -018, the manual sampling instructions, issued